用語の統一

”earth reinforcement”をメインに使い、小さな要素のような記述（例えば、室内実験記述など）に”soil reinforcement”を使用する。

2020.8.25修正

Chapter 6 Earth Reinforcement

Abstract: In this chapter, first the concept of earth reinforcement as a method to improve ground is described. The basic principles of earth reinforcement is then described. A brief description different types of geosynthetics products are given. The focus is mainly on the geosynthetics and Nailing and Anchoring, which are widely used in various ground improvement projects.

Key words: Geosynthetics, Geotextile, Geogrid, Nailing, Anchoring,

  - Introduction

French architect H. Vidal was the inventor of concept of modern reinforced earth. Vidal (1966) introduced the basic mechanism underlying reinforced soils behaviors. Much of the current development can be contributed to the pioneering work. The concept of earth reinforcement is based on the existence of strong soil-reinforcement interaction (like roots of a tree) due to their tensile strength and frictional or adhesional properties. Such reinforcement techniques are therefore, used in various geotechnical structures: e.g, slopes and embankments, retaining walls, foundations, dams etc. In recent years, such concept also led to techniques of using trees in slopes to reinforce the soils (Yamamoto et al, 2017). The past four decades have experienced a tremendous development in soil reinforcement as compared to the other ground improvement techniques. Many of those techniques can be found in Ochiai et al (….IS Kyushu…)

追加記述を要す

6.2. Ground Reinforcement Vs Ground Improvement

Fig.6.1 (JGS, 2009) shows ------

削除する

追加記述を要す

6.2.1 Difference between ground reinforcement and ground improvement

The difference between ground reinforcement and ground improvement is summarized in Fig.6.2 (JGS, 2009). It can be defined that ground improvement is to stabilize unstable ground using the methods such as replacement, solidification and mixing and that ground reinforcement is to draw the strength of the ground by other materials being laid on or inserted into it, without changing its soil properties.

6.2.1 Mechanism of ground reinforcement

H. Vidal (1966) was the first to propose a general and realistic concept of reinforcing soils. Following his pioneering research, Schlosser and Long (1972) proposed the mechanism of reinforcing earth based on the concepts of anisotropic cohesion and enhanced confining pressure. Test results by Schlosser and Long (1972) have indicated that the reinforced soil has higher strength than unreinforced plain samples as shown in Fig. 6.3 (Schiosser et al, 1972). As seen in Figure, the failure of the reinforcement can take place in two ways: (1) failure by slippage of the reinforcement at low confining pressure and (2) failure by breakage at high higher confining pressure. Thus, the reinforced sand behaves as a cohesive materials having the same friction angle as the original sand, and an anisotropic pseudo-cohesion due to reinforcement is generated as shown in Fig.6.4 (Schiosser et al, 1972). The pseudo-cohesion is rapidly mobilized at low axial deformations. As seen from that Figure, Mohr’s circle of stress is shifted due to reinforcing of the soil mass, while the failure envelope remained the same for both reinforced and unreinforced samples. Such effect is called the enhanced confining pressure effect.

In his Keynote address in the 11th International Conference on Geosynthetics (11ICG) at Seoul, Korea, Prof. Ziegler described the mechanism of improvement as a result of micro scale interaction and macro scale interaction. He divided the mechanism into three parts: pullout effect, confining effect and membrane effect (Fig.6.5). According to this definitions, the mechanism depends on the applications. Pull out effect will be dominant in applications such as retaining structures (passive zone) and anchor trenches. Confining effect will be dominant in application such as base reinforcement, foundation pads and retaining structures (active zone). On the other hand membranes effect will determine the improvement in applications such as foundation on piles in soft ground and overbridging sinkholes.

6.3 Types of Reinforcing Materials and Methods

There are three categories of literature available, which are relevant to the research on earth reinforcement.  They are: 1) types of reinforced soil structures (e.g., foundations, embankment, retaining walls, slopes and excavations), 2) development of the components of reinforced earth and 3) analysis and design of the reinforced earth structures. Two groups of reinforcements, extensible and inextensible exist (McGrown et.al, 1978; Bonaparte and Schemertmann, 1987). The two categories of reinforcements mentioned above can be described as follows.

Inextensbile reinforcement is a reinforcement used in such a way that the tensile stain in the reinforcement is significantly less than the horizontal extensions required to develop an active plastic state in the soils. Such reinforcement materials are so stiff that the equilibrium is achieved at virtually zero horizontal extensions.

Extensbile reinforcement, on the other hand, is a reinforcement used in such a way that the tensile stain in the reinforcement is equal to or larger than the horizontal extensions required to develop an active plastic state in the soils. Such types have very low moduli, and virtually no tensile forces are introduced to the soils mass at the strain required to develop an active plastic state.

Therefore, steel reinforcements such as nailing and anchoring can be considered as inextensible reinforcement, while geosynthetics reinforcing materials (described in detailed below) can be considered as extensible reinforcements.

Inextensible reinforcement leads to series failure (Fig.6.6 (a)), while extensible reinforcement results in parallel failure as shown in Fig.6.6 (b).

Reinforced soil structures can be grouped into three classes (Ingold, 1982).

- Embankments/Retaining Walls: A primary role of reinforcement in an embankment or a retaining wall is to support the lateral pressure in the fill while maintaining the full bearing capacity in the foundation (Fig.6.7). The reinforcement provided at the embankment base prevents lateral displacements of the embankment and foundations soils, subsequently the bearing capacity of the soft soil and the stability of the embankments are increased.

- Subsoil Reinforcement beneath Foundations: The function of an effective reinforcement is to hold the zones together in the case of a footing (Fig.6.8).

- In-situ Reinforcement (Soil Nailing): Soil nailing is used to stabilize the natural slopes, cuts or excavation, wall in stiff clays, granular soils and soft rocks. The nails are usually steel rods 20 – 30 mm in diameter that are inserted into soils either by simple driving or by grouting in pre-drilled borehole (Fig.6.9).

6.4 Geosynthetics

6.4.1 Description

The geosynthetics products family include various products of the textile, rubber and plastic industries as well as bitumen-polymer membranes and bentonite industries. The different polymers commonly used for the manufacturing process of geosynthetics are: polyethylene (PE), polypropylene (PP), polyester or polyethylene terephthalate (PET), polyvinyl chloride (PVC), polyamide (PA) and ethylene propylene diene monomer (EPDM).

Table6.1(1),(2)の分類は妥当か？

写真4点程度挿入するか？

Fig6.10, 6.11, 6.12を追加

Different types of geosynthetics are available in the market these days. They are: geotextile (GT), geogrid (GG), biotextile and biomat (BT), geomat (GA), geocell (GL), geonet (GN), geosynthetic for drainage (GCD), geosyntheic clay liner (GCL), geomembrane (GM), synthetics geomembrane (GMS), bituminous geomembrane (GMB). The symbols inside the parenthesis used above are suggested by the International Geosynthetics Society (IGS). They are prefabricated and come in rolls (height generally between 1 to 6 meters) or sometimes in panels. Each of the above is briefly described in the following (Table 6.1(1) – 6.1(2)).

Table 6.1 (1) Definition of Geosynthetics – Single Type

(Reference: Catalogue of BE-MA Editrice, 2018/2019)

| Name | Types | Definitions |
| --- | --- | --- |
| Geotextiles (GT) | Nonwoven geotextiles | NGTs are flat structures consisting of synthetic fibers causally arranged and made to adhere with mechanical or thermal. |
|  | Woven geotextiles | WGTs are flat and regular structures formed by the weaving of two or more series of synthetic fiber threads: warp yarns and welt yarns that allow to get regular, small-sized openings. |
| Geogrids (GG) | Extruded geogrids | EGGs are flat structures in polymer that are extruded and then pulled: this may only be done in one direction or in the two main directions. |
|  | Woven geogrids | WGGs are flat structures in the shape of a net made of high module synthetic fibers coated with a further protection layer. |
|  | Bonded geogrids | BGGs are flat structures where two or more series of fibers or other synthetic elements are linked at regular intervals by means of bonding. |
| Biotextiles and biomats (BT, BM)) | Boitextiles | BTs are made of natural fibers assembled to form a flat structures open and deformable. |
|  | Biomats | BMs are made of natural fibers usually sandwiched nets in synthetic materials. |
| Geomats (GA) | GAs are made of synthetic materials filament, tangled together to form a highly deformable layer 12-20 mm thick, featured by a very high porosity. |  |
| Geocells (GL) | GLs consist of juxtaposed cells either assembled or produced with strip of extruded synthetic materials, approx. 100 mm high, to form a honey-comb structure. |  |
| Geonets (GN) | GNs are meshes made up or two overlapping series of threads that cross at a constant angle in order to form constant and regular opening (by extruding thermoplastic polymer and welding of two series of threads). |  |

Table 6.1 (2) Definition of Geosynthetics – Combined Type

(Reference: Catalogue of BE-MA Editrice, 2018/2019)

| Name | Definitions |
| --- | --- |
| Geosynthetics for drainage (GCD) | GCDs may be made of homogenous elements or, vice versa, by composite elements. Homogeneous elements: moulded synthetics with a special profile Composite elements: a geonet layer sandwiched between two layers of geotextiles. |
| Geosynthetic clay liners (GCL) | GCLs consist of a thin layer of swelling clay between 2 layers of geotextile or glued to a synthetic geomembrane. |
| Synthetic geomembranes (GMS) | GMSs are either homogeneous or reinforced depending on whether there is or not a (synthetic or metal) reinforcing element inside its thickness. GMSs are of plastomeric or elastomeric type. |
| Bituminous geomembranes (GMB) | GMBs are sheets with thickness ranging between 3.0 and 6.0 mm, and width varying between 1.0 and 1.5 m, produced by working a melted mix (bitumen, plastomeric, elastic polymer, mineral fillers etc.) and featured by small permeability coefficients. |

追加文章

Typical applications from Table6.1 and 6.2 are shown in Fig.6.10, 6.11 and 6.12.

？

In recent years another types of geosynthetics products have been making inroad Geointo the construction industries, which may be called three-dimensional geosynthetics due to their three dimensional reinforcing mechanism. They include EPS (Expanded polystyrene) shown in Fig.6.13 and TDGM (Tire derived Geo-materials) shown in Fig. 6.14. For the former, the readers are referred to Horvath (1995), while for the later the readers are referred to the Keynote paper (Hazarika et al, 2017) at Indian Geotechnical Conference and also is briefly discussed in Chapter.7 of this book.

6.4.2 Applications

The geosynthetics products find varieties of applications in geotechnical works. They include: roads, railways, retaining structures, reinforced embankments, drainage systems, tunnels, dams, reservoirs, canals, landfills and sludge containments.

6.4.3 Construction Procedures

There are various types of reinforced earth methods, but the construction procedure of the most popular reinforced soil wall (Vidar, who advocated the reinforced soil as a modern method, named it Terre Armee) will be described. Fig.6.15 shows a cross section of the reinforced earth wall. The structures combine selected and controlled granular backfill with steel flat bar or geosynthetic tensile reinforcements and a modular facing system, generally comprised of precast concrete panels, welded wire mesh or semi-elliptical steel panels. This can be adapted to suit retaining walls of any height. It is also capable of supporting major dead and live loads imposed by the associated structures, vehicles or other equipment.

Fig.6.16 shows the construction procedures of Terre Armee (Fig.6.15) which has concrete skins and it follows the compaction method (Section 2.2) basically. Soil materials should be spread at the thickness of 10-30 cm and compacted by rolling machines which are driven in the parallel direction to the concrete skin wall. Generally, tire rollers or vibratory rollers with 8 - 20 ton capacities are used and soil layers near concrete skins should be used vibrating compacters (1 ton capacity). In the installing depth of the reinforcement material (strips), it is based on the design value, but the rolling by the construction machines should be applied on the soil layer of the thickness above 15 cm.

6.4.4 Planning and Designing of Geosynthetics Reinforced Structures

Planning and designing of reinforcing earth structures using geosynthetics require the following to be known beforehand (Rowe, …).

- State of stress within the reinforced soil mass

- State of strain in both the soil and the reinforcement

- Axial force distribution in the reinforcement

- Horizontal soil pressure acting at the back of the reinforced soils mass and the vertical soil pressure at the base

- Vertical soil stress at each reinforcement layer

- Horizontal soil pressure acting on the face

- Horizontal and vertical forces transferred to the wall face

- Horizontal deformation of the reinforced soil mass

- Effect of varying design parameters (i.e. reinforcement stiffness, soil properties, facing stiffness, foundation stiffness, surcharge conditions, construction procedures etc.) on the response of the system

6.5 Nailing and Anchoring

Table6.2 修正済み

Nailing and anchoring is the inextensible type reinforcement in which steel bars are used to reinforce soils which are natural grounds. Natural ground reinforcement methods are cited by way of three functions of nailing, bolting and anchoring (Table 6.2).

Table 6.2. Natural ground reinforcement methods (         )

| Function | Method | Objective Ground | Used materials (Usual case) |
| --- | --- | --- | --- |
| Nailing | Soil nailing Micro-piling Doweling | Soil | Steel reinforced bar Cement grouting Shotcrete Retaining wall (if necessary) |
| Bolting | Rock bolting | Rock |  |
| Anchoring | Ground anchoring (or Earth anchoring) | Soil & rock | Steel wire, Steel rod Anchorage, Bering plate |

Nailing is classified to three methods on the slenderness ratio of rebars and the action of reinforcing materials (Fig.6.17). Soil nailing, Micro-piling and Doweling are the geotechnical methods to improve the bearing capacity of natural ground, the stability of the slope and the reduction of earth pressure. The reinforcement materials (generally: steel rebar) are arranged and inserted in the natural ground (usually: with drilling works), and they are bonded their entire length by cement grouting. The resistant force (tensile, bending and shear stress etc.) between the reinforcement materials and grounds is generated passively by the movement of ground.

Whereas, rock bolting2),3) is a method of rock reinforcement used to stabilize the cutting rock slope or the excavated rock face in underground mines and tunneling, and also to prevent rock-fall. Rock bolt transfers load from the unstable exterior, to the confined interior of rock mass. The combination of rock bolting, wire meshing and shotcrete is used in the New Austrian Tunneling Method (NATM), from which soil nailing evolved. In general, rock bolts work by knitting of the rock mass together sufficiently before it can move enough to loosen and fail by unravelling. The installation of rock bolts can be achieved either manually with stoppers and impact wrenches, or mechanically with pneumatic bolting equipment. The fixing methods of rock bolts and rock mass are applied by mechanical-anchor bolts, cement-bonded bolts and resin bolts. Mechanical-anchor bolts utilize an expansion shell to secure an anchoring point at the end of a drill hole in stable ground. Resin bolts and cement-bonded bolts differ in that they rely on the bonding property of resin or cement to transfer rock loads. Rock bolting is generally applied for tunneling, and its design method is established by Rock Quality Designation (RQD) on Rock mechanics. Therefore, details of Rock bolting is not described in this book.

Anchoring for natural ground is called as “ground anchor or earth anchor”, which is used for tensile stress and transmits the force from a structure to the ground in which they are anchored (as follows: “ground anchor” will be used terminologically). Ground anchor consisting of cables or rods connected to a bearing plate are often applied for the stabilization of steep soil slopes and rock slopes, increase of bearing capacity of soil stratum and prevention of landslides etc. Fig.6.18 and Fig.6.19 shows a typical application of ground anchor and details of its composite elements which are made up of anchorage, cable and sheath or sleeve.

6.5.1 Soil Nailing

6.5.1.1 Description

ハザリカPPTの図面？ここに図を追加すると以下の図の番号が変わる

Soil nailing is a technique used to bring soil stability in areas where slope failures/landslides might be a problem. Soil nail can prevent slope failures and landslides by inserting steel reinforcement bars into the soil, and anchoring them to the soil strata. It is called Soil Nail, because it’s like having a nail being hammered into the soil, where the nails, are the steel bars. Various component of soil nailing is shown in Fig. ***(PPT).

This type of ground reinforcement technique has the following advantages:

1) It is ideal for tight spaces,

2) Less noise and fewer traffic obstructions,

3) Less impact on surrounding areas,

4) Lower load requirements than tieback anchors systems,

5) Eliminates the time and expense of placing steel piles,

6) Can be used to repair other existing wall systems,

7) It can be used on new constructions, as temporary structures or on

remodeling process,

8) Wall height is not restricted,

9) Reduced right-of-way requirements.

On the other hand it has some disadvantages as well which are as following:

1) Sand and gravels might not be compatible with soil nailing,

2) Not recommended to use in areas of high water table,

3) Soil nailing in very low shear strength soil may require a very high soil nail

density,

4) Soil nailing in sensitive soils and expansive soils for permanent long-term

applications is not recommended,

5) Specialized contractors are needed to perform the work

6.5.1.2 Applications

Soil nailing is applied for the purpose of stabilization of natural earthen slope and cutting earthen slope, or for the purpose of strengthening of bearing soil layer. Characteristics of soil nailing are as follows:

1) The labor-saving construction system is applied in this method, because reinforced materials and the usually used equipment are small-scale and light-weight.

2) The gradient of earthen slope can be cut by this method steeper than the gradient of natural slope.

3) The reverse concreting excavation method can be applied for the slope cutting.

4) If the ground deformations or the ground displacements are observed under construction, it’s possible to raise safety by increasing of rebars.

6.5.1.3 Construction procedures

The construction of soil nailing usually involves the following procedures.

- Drilling into the soil, where the nail (steel bar), is going to be placed.

- After the drilling has been completed, depending on the exact depth provided by the geotechnical engineer, the nail is inserted into the drilled hole.

- Then, it is grouted into the soil to create a monolithic structure

- After placing the nail, a shotcrete layer is usually placed as a facing material.

Usually, the objective ground is drilled by boring machine and the rebar is inserted into the bore hole. Then it is bonded along its entire length by cement grouting with some additives. In the case of cutting slope stability, the cutting surface will be covered by the shotcrete lining to accomplish the unification of soil mass, rebar, grout and lining (Fig.6.20). It is likely that isolated soil nail head plates may be used at the surface.

Under certain circumstances, hollow-systems steel bars are available. Hollow bars may be drilled and grouted simultaneously by the use of sacrificial bit and by pumping grout down the hollow bar as drilling progresses.

6.5.1.4 Planning and Designing

Nailing are classified three categories as mentioned above, but soil nailing will be described on behalf of them.

Usually the rebar is used with steel bars 3〜10m long of 16〜50mm dia. A drilled hole is 60〜150mm dia. Nail spacing is 0.5 〜1.5m. Rebars are installed at a slight downward inclination with rebars installed at regularly spaced points across the slope face. Table 6.3 shows the favorable soils and unfavorable soil for soil nailing.

At designing of soil nailing, two steps should be done, which are the internal stability for reinforced masses and the structural stability of pseudo-retaining-wall made up of reinforced masses.

Table 6.3 List of favorable and unfavorable soils for soil nailing (         )

| Favorable soils | Unfavorable soils |
| --- | --- |
| Stiff to hard fine-grained soil Clayey silts Silty clays Sandy clays Sandy silts Sand and gravel which are dense Weathered rock Glacial soils | Dry, poorly graded cohesion-less soils Soils with a high groundwater table Soils with cobbles and boulders Soft fine-grained soils Highly corrosive soils Weathered rock with weakness planes Loess |

ハザリカPPTの図面？ここに図を追加すると以下の図の番号が変わる

6.5.2 Anchoring

6.5.2.1 Description

Anchors are stabilization and support elements that transfer tension loads, using high-strength steel bars or steel strand tendons. Elements of an anchor are shown in Fig. ** (PPT). They include anchor head, anchor frame, anchor rod and the grouting mass. An anchor can either active or passive. An active soil anchor is pre-tensioned before it takes up the load, which is a means of limiting deformation. A passive soil anchor is tensioned as the structure itself applies load to it. It does not usually have a free length

ハザリカPPTの図面？ここに図を追加すると以下の図の番号が変わる

of tendon (it is grouted over its whole length) as shown in Fig. ***(PPT).

6.5.2.2 Planning and Designing

不要？

Ground anchors consisting of cables or rods connected to a bearing plate are often used for the stabilization of steep slopes, the prevention of landslides and supporting of earth retaining walls etc. Fig.6.17 shows an illustration of conventional anchoring, which consists of anchor head, tension part and anchorage part.

As follows, the stability analysis of slope, which is reinforced with ground anchor, is shown (Based on Swedish slice method, Fig.6.21).

P: Designed anchoring force (kN/m) to get the required safety factor FS)

FS: Required safety factor of sliding failure on reinforcement by anchoring

ΔP: Anchoring force which act for each slice (kN/m)

ΔW: dead load (kN/m) of each slice

ά: Angle of sliding plane and horizontal plane (°)

β: Angle of direction of anchor force and sliding plane (°)

φ: Internal friction angle of soil (°)

c: Cohesion of soil on sliding plane (kN/m)

Δl: arc length on sliding plane of each slice (m)

If the calculated anchoring force is divided by number of placed rows and anchor horizontal interval, the designing anchor force per an anchor will be obtained. The plane arrangement of anchors is planned at 1.5 m – 3.0 m grid pattern, empirically. The angle for driving and placing of the anchor is generally over 15 degree with horizontal level.

After then, the pulling resistant force of anchor is calculated by the following formula:

T: Ultimate anchoring force (kN)

D: Diameter of anchorage (m)

L: Length of anchorage (m)

τ: Ultimate bonding force or ultimate friction force between grouting materials and ground (kN/m2)

6.5.2.2 Application

Earth anchoring are typically used in geotechnical construction projects, and have a variety of applications, including (Wikipedia 2019):

- Supporting tools for retaining walls, as part of excavation systems.

- Structural support of temporary buildings and structures

検討を要す

Tethering marine structures, such as floating docks and pipelines.

- Supporting guyed masts, such as radio transmission towers.

- Anchoring utility poles and similar structures.

- Drainage systems, for load locking and restraining capability to happen simultaneously.

- Landscape, anchoring trees, often semi-mature transplants.

ハザリカPPTの図面？ここに図を追加すると以下の図の番号が変わる

6.5.2.3 Procedures

The construction of anchoring usually involves the following procedures (Refer to Fig. *** PPT).

- A full-length hole is drilled through the soil and into the bond zone in soil or rock using casing if necessary.

- Thread bar or strand tendon is inserted into the hole and the hole is filled with high-strength grout.

- Any casing used is then extracted.

- The length of bar or strand above the bond zone is covered by a bond breaker to eliminate load transfer above the bond zone.

- The anchor head is then generally tensioned and connected to the structure requiring the support.

Referencesの空きを埋める必要がある

References

BE-MA Editrice (2018/2019): Directory of geosynthetics (Catalogue), Italy.

Bonaparte, R. and Schmertmann, G.R. (1987): Reinforcement extensibility in reinforced soil wall design, Proceedings of the NATO Advanced Workshop on the Applications of Polymeric Reinforcement in Soil Retaining Structures, Kingston, Canada, pp. 365-407

Fukuda, N., Yamanouchi, T., and Miura, N. (1989): Comparative Studies of Design and Construction of a Steep Reinforced Embankment, Geotextile and Geomembranes, Vol.4, pp.269-284.

Hazarika (2017)

Horvath (1995)

Ingold, T.S. (1982): Reinforced Earth, Thomas Telford Ltd., London.

JGS Report (2009): Technical committee No. 17 on ground improvement, International Society for Soil Mechanics and Foundation Engineering (ISSMGE), Retrieved from www.bbri.be/go/tc17

JGS 地盤工学会の設計施工指針

Jones, C.J.F.P. (1992): Economic construction of reinforced soil structures, Proceedings of the International Symposium on Recent Case Histories of Permanent Geosynthetic-Reinforced Soil Retaining Walls, Tokyo, Japan, pp. 103-106.

McGrown, A., Andrawes, K.Z., and Yeo, K.C. (1978): Effect of inclusion properties on the behavior of sand, Geotechnique, Vol. 28 (3), pp. 327-346.

Ochiai et al

Rowe

Schlosser, F., Jacobsen, H.M., and Juran, I. (1981): Soil Reinforcement- General Report, Proceedings of the Eigth European Conference on Soil Mechanics and Foundation Engineering, Helsinki, Finland, Vol. 3, pp. 1159-1180.

Vidal, H. (1966):

Vidal, H. (1978): The Development and Future of Reinforced Earth, Keynote Lecture, Proceeding of the Symposium on Earth Reinforcement, ASCE, Pittsburg, USA, pp. 1-61.

Wikipedia: Soil nailing, Wikipedia, Last modified on 1 October 2016.

Wikipediaからの引用方法、表示方法を検討する

Wikipedia: Rock Bolting, Ritchie Wiki, Last modified on 24 November 2009.

Wikipedia: earth anchor https://en.wikipedia.org/wiki/Earth_anchor（2019.8.6）

Wikipedia: Rock bolt, Wikipedia, Last modified on 18 April 2016.

Yamamoto, K., Teramoto, Y., Hira, M. and Nagakawa. K. (2017): Site Investigation and In Situ Testing on Shallow Landslide Scars of Natural Slopes Covered by Volcanic Ash and Pumice Fall, Proceeding of Geotechnical Hazards from Large Earthquakes and Heavy Rainfalls, Springer

Zeigler, M. (2018): IGS Seoul Keynote Paper (Paper 2)

Questionnaires – Practicing what you have learned.

6.1 What is the most effective way to Reinforced fine soils like clay?

For example could strip reinforcement used for fine soils??? As reinforced walls should be backfilled with coarse materials like coarse sand or gravels

# 6.2 Can we remove OH compound from any fiber material chemically?