Chapter 4 Ground Improvement with Admixture or Inclusion

Abstract: In this chapter, the techniques of Ground Improvement with admixture or inclusion. Specifically, Surface compact using cement and lime, Sand compaction pile and Stone column are described. They are consisted of procedures by adding some chemical solidifying materials in soils and by including other materials into the ground.

Keywords: Soil-cement, Soil-lime, Sand compaction pile, Stone column,

4.1 Introduction

Ground Improvement with admixture or inclusion is the improvement method in which either admixtures such as cement and lime or inclusions such as sand or crushed stones are used in the ground. Basically three different techniques are available: 1) Surface compact using chemical solidifying materials such as cement and lime, 2) Sand compaction pile using inclusion made of sand and 3) Stone column using inclusions made of crushed stone.

Soil-cement is a mixture of pulverized soil and Portland cement with some water, compacted to high density. As the cement hydrates, the mixture becomes a hard and durable soil mass. The soil materials can be almost sand, silt, clay and gravel.

Lime is the oldest traditional stabilizer used for soil stabilization. The mechanism of Soil-lime treatment involves cation exchange, which leads to the flocculation and agglomeration of soil particles. Soil-lime effectively increases the strength, durability and workability of the soil. Such treatment also improves soil compressibility.

Sand Compaction Pile method is used frequently in construction to form compacted sand piles by vibration, dynamic impact or static excitation in soft ground. This method improves stability or compressibility and prevents liquefaction failure in loose sand, the SCP method is now often applied to soft clay ground to ensure stability and reduce ground settlement.

Stone column is an array of crushed stone pillars placed with a vibrating tool into the ground below a proposed structure. Such techniques increase the load and drainage of the soil while reducing settlement and liquefaction potential.

4.3 Sand Compaction Pile Method

4.3.1 Description

Sand compaction pile is a method, in which dense and compacted sand piles with expanded diameter are driven and placed in the ground by using vibration or hammering. This method is applied for the purpose of improving loose sandy ground or soft clayey ground by inserting sand piles.

When sand compaction piles are applied for loose sandy ground, the ground will be compacted by the pressurizing effect of sand piles. The shearing resistance of the ground will be increased due to decrease of the voids within soil mass. Liquefaction of ground during earthquake can be prevented using sand compaction piles, through reduction of the liquefaction potential of loose sandy grounds. Fig.4.7 (Takahashi, 2008) shows a typical example of liquefaction prevention of foundation soils in case of quay wall. On the other hand, when sand compaction piles are placed in soft clayey ground, the ground will be improved by the forced replacement of soft soils and the consolidation effects due to drainage function of sandy inclusion. The bearing capacity and the shearing strength of soils will be increased as the composite ground from the view point of theoretical geo-mechanics. Fig.4.8 (Takahashi, 2008) shows an adopted example of this method with the purpose to improve soft clayey ground when constructing road embankment.

4.3.2 Principle

Sand compaction pile (hereinafter SCP) is used to improve ground stability by installing large diameter compacted sand piles in the ground. These sand piles mobilize large shear strength due to formation of composite ground. This mechanism improves the ground through increase of bearing capacity and factor of safety of slope. Due to their stress redistribution effect, sand piles are able to increase the bearing capacity of composite ground consisting of sand and clay and thus, can reduce the amount of ground settlement.

Fig.4.9 (Fudo, 1971) shows the principle of ground improvement for sandy soil using Sand compaction pile. As shown in Fig. 4.9a, if the void ratio of original ground is e0, the volume of it can be expressed as (1+e0). If the amount of sand corresponding to Δe is pressed into this ground, the void ratio will be reduced by that amount. The decrease in void ratio is evaluated as the improvement effect. The ratio of the amount of pressed-in sand to the volume of the original ground is called the replacement rate (as), which is in principle is nothing but the degree of ground improvement, and is expressed by the following equation.

(4.1)

The replacement rate can also be expressed by the cross sectional area ratio of sand piles to be driven against the objective ground area. Fig.4.10 (Fudo, 1971) shows Plane arrangement of SCP, which are illustrated in (a) square pattern, (b) equilateral triangular pattern and (c) parallelogram pattern. In each case, replacement rate (as) is expressed by the following equation.

(a) and (c) Square and Parallelogram (rectangular)

(4.2)

(4.3)

(b) Equilateral triangular

4.3.3 Procedure

Sand compaction piles consist of driving a hollow steel pipe down to the required depth. The bottom of steel pipe is closed by means of a freely movable plate. The hollow pipe is filled with sand, and thereafter, the pipe is withdrawing the pipe while air pressure is directed the sand inside it.

Fig.4.11 (Yasuda et al 1996) shows the general procedures for SCP method, which consist of re-driving and compaction process. After penetrating a casing into the ground, sand is filled into the casing. Then by withdrawing the casing, the sand is discharged into the bored hole and then compacted by vibration. The surrounding subsoils are also compacted during this process. Usually, when a 50 cm diameter casing is used, the compacted sand pile diameter will be 70 cm. The spacing between each sand compaction pile varies from 1.2 m to 3.0 m.

4.3.4　Design procedures

- In the case of sandy ground

Various design methods have been proposed for applying SCP to sandy ground. The following three means are proposed for its design, when applying it for sandy soil.

ⅰ) Using charts, which are based on N values from case histories,

ⅱ) Using charts, which are based on relationship amongst N values, Dr and e,

ⅲ) Consideration of the fine fractions of original ground.

Herein, the conventional design procedure based on N values, which is considered to be the simplest in many applications, is described.

Fig.4.12 (Fudo,1971) shows N-value after being improved by SCP, which is based on the data from the past case histories. N0 on the horizontal axis shows the ground strength before the construction of SCP, and N1 on the vertical axis shows the ground strength after the improvement by SCP, which were measured between the sand piles. This figure is summarized with as indicated as a parameter. In this figure, parameter as is referred to the replacement rate of sand piles and is expressed by Equation 4.1 stated in the previous section. An example of the design is shown in Fig. 4.13 (Fudo,1991).

(4.4)

Where, A: sharing area per one sand pile

ｄ：spacing of sand piles

r:  radius of sand pile

e0：void ratio before improvement

e1：void ratio after improvement

If the simplified figure (Fig. 4.12) is used, the desired replacement rate can be obtained at the intersected point of N0 of the original ground and the target N1 after improvement.

- In the case of clayey ground

For the clayey ground, casing pipes are installed in the ground down to the designated depth at uniform intervals. When SCP is applied for the soft clayey ground, the concept of composite ground is required for designing.

Harada Kobayashi Fig. 1 here and explain

In case of bearing capacity of composite ground, the following procedure was proposed by Suematsu (1991), which is explained in Fig. 4.14 (Suemat	su, 1991)

(4.5)

(μc: coefficient of stress reduction)

(μs: coefficient of stress concentration)

Where as：replacement rate of sand piles,

Aｓ:plane area of sand piles,

Ac: plane area of clayey ground

c:

s:

:

（正しいかどうかCheckをお願いします）

A parameter m is the stress sharing ratio and Table 4.4 shows the relation between the replacement ratios as, the internal friction angle φ of sand and the stress sharing ratios m.

Table 4.4 Relation of as, φ and m (Fudo, 1971)

| as | φ | ｍ |
| --- | --- | --- |
| - ～0.3 0.3～0.7 0.7～ | 30° 30° 30° | 3 2 1 |

Fig.4.15 (Suematu, 1991) shows the evaluation of the shear strength of composite ground assuming slip failure. The shearing strength τsc of the composite ground can be expressed by the following equation.

(4.6)

4.3.5 Applications

Table 4.5 shows the relationship between the soil types and aims of ground improvement by SCP.

Table 4.5 Relation between soil type and Aims of improvement by SCP (Fudo, 1971)

| Soil type Aim of improvement | Very soft clay | Soft clay | Loose sand | Alternation of sand and clay |
| --- | --- | --- | --- | --- |
| Increasing of bearing capacity Reinforcing of shear strength Increasing of lateral resistance Prevention for ground settlement Countermeasure for liquefaction | ◇ ◇ ◇ | ◇ ◇ Δ ◇ | ◇ ◇ ◇ ◇ | ◇ ◇ ◇ Δ Δ |

(Notes)   ◇: dominant   Δ:rare

There are many case histories such as embankments, foundations of oil tanks, port and harbor facilities, buildings and so on, in which this method was applied for ground improvement. A typical application from Japan is described below.

SCP was applied as liquefaction countermeasure of the revetment of a sewage plant in Yokohama coastal area in 2009 (Fig.4.16- JAFEC, 2016). Fig. 4.16(a) shows the quay wall and the foundation details of this project.  In this project, the average N-value of the original ground was 7, the target N-value after improvements was set to 10 or more. After improvement works, the N-values between the each pile was measured, which are shown in Fig. 4.16 (b). As displayed in the figure, the average N-values increased to more than 15 after the execution of SCP.