Chapter 5 Ground improvement with grouting type admixture

Abstract: In this chapter, the techniques of Ground Improvement with grouting type admixture are described. Particulate grouting, Permeating grouting, Compaction grouting,Jet grouting and Deep-mixing are described. These methods are normally carried out by boring holes into the ground, and then pumping the grout solution at high pressure through inserted pipe, tube or special designed wings. Grouts can be of cement, silicate, or other chemical materials and solidification materials.

Keywords: Grouting, Particulate grouting, Permeation grouting, Compaction grouting, Jet grouting, Deep mixing,

5.1 Introduction

Ground improvement by injecting grouting type admixture into the soils is called Grouting method, which is normally carried out is by boring holes into the ground, and then pumping the grout solution at high pressure through inserted pipe or tube. Grouting, as is normally called, is a technique to inject various types of grouts into the ground at a deliberately controlled pressure and flow rate. Grouts can be of cement, silicate, or other chemical materials, which are selected to suit the particular ground conditions and improvement objectives. In the early 1800s, this method was mainly executed by injecting clay and natural cement into gravelly ground and letting those permeate into the soil pores to produce a solidified soil-grout mass. Grouting method with cement milk or clay slurry was developed after that and applied for ground improvement with various purposes. The method, however, has some drawbacks: notably the inability of the grout to permeate in clayey soils and non-uniform formation of solidified ground mass. To overcome those drawbacks, Deep mixing method was developed in the 1970’s and Jet grouting method was developed in the 1980’s. Many effective advantages of these methods are widely seen now a days, due to improvement of the equipment and materials for these methods.

Figs. 5.1 show the categorization of various grouting techniques and the approximate compressive strength of the solidified soil mass obtained using each method.

5.2 Grouting method (Particulate grouting, Chemical grouting)

5.2.1 Description

Originally, Grouting was adopted as geotechnical means to prevent groundwater leakages and ground collapses during the excavation work. Thus, it was primarily used either to make the ground impermeable or to increase the ground strength.

Grouting is often applied to improve the ground underneath existing structures such as large oil tanks, railroad tracks and others. Directional drilling technique is often employed for drilling boreholes to circumvent underground obstructions to reach the target improvement zone.

The standard Grouting system is shown in Fig. 5.2. The grout is mixed in the mixing plant and transported into the injection pipe by the grout pump. After that, the grout is permeated into the ground from the tip of injection pipe. Generally, the grout is mixed with multiple materials and is chemically treated to obtain a solidified mixture in the ground. Multiple materials are mixed to obtain the solidified mass through chemical reaction, but each chemical reaction time differs depending on each combination. As shown in Fig. 5.2, there are three mixing positions for the multiple materials: (a) the exit of mixing plant, (b) the inlet of swivel and (c) the tip of injection pipe. Those positions are determined by the reaction time of those materials.

Define what is grout: …….

The materials used as grout can be broadly divided into three as shown in Fig. 5.3. They are (1) suspension grout, (2) solution grout and (3) others.

Suspension grout is a heterogeneous mixture containing solid particles that are sufficiently large for sedimentation, and is classified on the basis of the dispersed phase and the dispersion medium. In the case of Grout, solid particles (dispersed phase) are cement-based materials and clayey materials, and solvent (dispersion medium) is water. The solidifying reactions on these materials depend on the hydration reaction of materials themselves.

引用ミスか勘違いのようです。「その中に分散状態を維持するために分散剤が混合されている」

Solution grout is a homogeneous mixture composed of two or more substances, in which some dispersants are mixed to maintain the dispersed state of the grout. There is a time gap between the mixing of solutions and the formation of jelly. The time taken to gel formation is called “Gel-time”. The semisolid material is caused by formation of a three-dimensional skeleton, which will act as a bonding force. In the case of solution grout, the solutions are further classified into water-glass type (sodium silicate) and the polymer type. The former can be of solution type and semi-suspension type. Polymer type solution grout is made of materials such as, acrylic amide, urea resin, urethane resin and silica resin, etc.

Table 5.1 shows the typical grouts and the names associated with those.

Table 5.1 List of Grouts

| Group names | Types | Names of grout |
| --- | --- | --- |
| Cementitious Particulate | Suspension | Cement Milk Cement-Bentonite Cement-Lime Cement-Slag Lime-Slag |
| Water glass (Sodium Silicate) | Semi-suspension | Water glass-Cement Water glass-Slag |
|  | Solution | Water glass-Acidic reaction agent2) Water glass-Alkali reaction agent3) Water glass-Metal salt reaction agent4) |
| Synthetic Polymer1) | Solution | Acrylic amide Urea resin Poly-urethane resin Others |
| ［Note］ 1) These grouts are being restricted for use as injection material, because unreacted substances of them may be toxic. 2) Sodium hydrogen carbonate, sodium hydrogen sulfate, phosphoric acid etc. 3) Sodium aluminate, ethylene carbonate, glyoxal etc. 4) Calcium chloride, aluminum sulfate etc. |  |  |

5.2.2 Principle and Mechanism

A. Strength and permeability of grouted soils

The ground improvement by grouting is to increase the cohesion of the targeted soil, but the improvement effects depend on characteristics and engineering properties of the targeted soil. In sandy soil, the increments of cohesion of grouted soils are roughly 50 - 100 kN/m2. In clayey soil, the increments are within the range of 10 -40 kN/m2. When grouting is performed to decrease the permeability of soils, the order of the co-efficient of permeability (k) can be reduced from -3 to -5.

B. Gel-times and Gel- properties of solutions

Gel-time refers to the time in which the solution-type grout loses its fluidity and increases its viscosity (which is called gelation). The grout which solidifies momentarily after mixing is called the flash gelling grout, and the grout which takes longer time for its gelation is called the slow gelling grout.

C. Pattern of injected zone

The pattern of injection determines the shape of the permeated and solidified mass obtained as a result of grouting. As shown in Fig. 5.4, the injection pattern can be divided into four types; a) Permeation injection, b) Split Injection, c) Split and permeation Injection and d) Boundary Injection.

- Permeation Injection: It is performed in highly permeable sandy ground, in which water or air in pore between soil particles is replaced by the grout. In the case of uniform sandy soil, it permeates into a spherical shape.

- Split Injection: In this type of injection, ground is fractured due to the injection pressure, and as a result, the grout permeates and solidifies into the veins by splitting. When permeation injection is difficult to perform in soils such as clay with low permeability, this method of injection is adopted.

- Split and Permeation Injection: This is the combination of permeation and split injection, in which ground splitting occurs due to the injection pressure, but only in the vicinity of injecting outlet. In the deeper part, grouting is done by permeation in horizontal direction

- Boundary Injection: This is the type of injection, in which the grout is permeated and solidified along the boundary of soil layers or existing structures in the ground.

5.2.3 Procedure

A. Particulate grouting (Suspension type grouting)

In the case of Particulate grouting (Suspension type grout), solid particles (dispersed phase) are cement-based materials and clayey materials, and solvent (dispersion medium) is water. The solidifying reactions on these materials depend on the hydration reaction of materials themselves, therefore this type of grout does not have the gel time and cannot be controlled. Since this is the suspension type grout containing solid particles, it renders low permeability to the objective ground. However, when the solidified mass is formed due to sufficient enough permeation, the strength of soils obtained are expected to be higher than the other methods of grouting. Ground with the particle sizes of ranging from 5mm (gravel) to 2mm (medium sand) is only suitable for this type of grout. This type of grouting is used for splitting veins in clayey ground and filling the cracks in gravelly ground. Recently, micro-fine cement grouting is developed for the extension of permeation grouting by using finer grout, which are capable of penetrating into the small voids of fine sands.

Compaction grouting is a special type of particulate grouting. It is used for settlement control, structure re-leveling and liquefaction countermeasure of ground (Fig. 5.5). Compaction grouting, in which a stiff mortar-like grout is injected at high pressure to displace and compact the surrounding soils, increases the density of soft or loose soils by controlling displacement. The grout is made of cement, aggregates and water, and its slump is specified to be less than 5 cm.

B. Chemical Grouting (Permeation Grouting)

Chemical grouting is the typical style permeation grouting, in which the injection of chemical solution is performed for bonding the individual soil particles. The chemical solutions consist of a base material that is mixed with a hardening agent, which is mixed to harden the soils at a predetermined rate, depending on the compounds and length of gel-time desired for a particular application. There are two procedures for executing chemical grouting as shown in Fig.5.6 & 5.7. One method uses boring rod as the injection pipe (single pipe system, twin pipe strainer system as seen in Figs. 5.7a to c). The other method consists of three steps: 1) the boring rod is pulled out after drilling, 2) an injection pipe is inserted into the bored hole, 3) and grouting is performed using the inserted injection pipe (double packer system, multi-bundle tube system as seen in Figs. 5.7c to d).

In chemical grouting two kinds of solutions need to be prepared: the base agent and the hardening agent. Solidification takes place when these two solutions are mixed. The gel-time of grout varies depending on their chemical compositions, combinations and concentrations. Depending on the gel time, the confluent position to mix two solutions will differ. Fig. 5.8 shows three different forms of grouting, depending on the gel time (slower to faster) of grouts and their mixing position (confluence point).

1) One-shot process: Grout solution with the base agent and the hardening agent at a predetermined mixing ratio are combined in the mixer or the inlet of the grout feeding pump. This process involves chemical mixing with the hardening agent in one mixer prior to injection. One-shot (slower) process is adopted for the grout with long gel time, for example, several tens of minutes.

2) One-half-shot process: Grout solutions with the base agent and the hardening agent are mixed in separate mixers and are fed in separate pipelines. Thereafter, they are combined at the swivel of injecting pipe and injected from the bottom. This process is adopted for the medium gel time of grout, for example, below 30 minutes.

3) Two-shot process: Grout solutions with the base agent and the hardening agent are

mixed in separate mixers and are fed in separate pipelines. Thereafter, they are combined at the bottom tip of the injecting pipe. This mean, in this process, the mixing

「瞬結」は”flash setting”と表現されている

and the injection of solutions are carried out at the same time. This process is adopted for the flash setting gel-time, for example, from a few seconds to several minutes.

In Table 5.2 the above three procedures are summarized.

| Name |  |  | Description |
| --- | --- | --- | --- |
| Single pipe | One-shot process |  | Grouts are injected with one solution prepared in one mixer, or grouts are prepared with two mixers and are combined at an inlet of the grout feeding pump. |
|  | One-half-shot process |  | Grouts are prepared with two mixers and combined at the swivel of injecting pipe and injected from the bottom tip of it. |
| Double pipe strainer | Single phase (One-half-shot process) |  | Drilling and injecting are carried out with the twin tubes which is equipped with strainers at the tip of them. Grout is injected by one-half-shot process as above-mentioned. |
|  | Dual phase |  | The first step is carried out by the grout with flash gelling time (split injection & two-shot). The second step is carried out by the grout with long gelling time (permeation injection & one-shot). |
| Double pipe with double packer | After drilling, the grouting outer pipe is inserted. Cement bentonite is filled up between pipe and ground for sealing around the pipe. Next, the grouting inter pipe with double packer is inserted in it. After then, cement bentonite is injected and the long gelling time grout is injected at second from the inter pipe (one-shot). |  |  |
| Multi-bundle tube (Multi-points grouting) | This method adopts an injection pipe bundled with 32 small diameter flexible tubes (φ: 6 mm). Flexible tubes are of varying length so that vents of grout are at different depth. At the same time grout is fed into each flexible pipe, so that injection at multiple points is possible at the same time. |  |  |

Table 5.2 Grouting style and grouting process

5.2.4 Design

1) Selection of Grout

The selection criteria of grout are shown in Table 5.3 and Fig. 5.9, according to applications. Depending on soil types, a suitable grout to be injected into that soil should be selected.

Table 5.3 Relationship between soil type and suitable grouts (JGS, 2009)

| Soil type | Material | Injection type | State of solidified mass |
| --- | --- | --- | --- |
| Sand, Sandy gravel, Gravel | Solution | Permeating | Voids between soil particles is filled with grout, and soil aggregate is massed. |
| Clay | Suspension | Splitting | Grout veins are formed in soil mass. |

From Table 5.3, it can be recognized that the pattern of injected zone and the suitable grout are different depending on whether the objective ground is sandy or clayey. Based on results of grain size analysis, the pattern of injected zone and the suitable grout should be selected according to percentage of sand and clay in the soils (Fig. 5.9). However, when dealing with gravelly soil with large pores, suspension grout is selected for filling those pores.

2) Selection of grouting procedures

Selection of a grouting procedure should be done after confirming the characteristics of each injecting procedure. Merits and demerits in case of Double pipe with strainer procedure and Double pipe with double packer procedure are shown in Table 5.4, The table also shows many applications in the most general form.

Table 5.4 Merits and defects of grouting procedure (JGS, 2009)

| Site conditions | Double pipe with strainer | Double pipe with double packers |
| --- | --- | --- |
| Ground without drilling obstacle Ground with drilling obstacle Objective depth for injection (under 25m) Objective depth for injection (over 25m) Near general structure Near significant structures Bottom improvement for open-cut Splitting grout for clayey ground Sandy ground under 10 N-value Ground with high permeability Waterproof for ground with high groundwater level | ○ ○ ○ ○ ○ | ○ ○ ○ ○ ○ ○ |

3) Quantity of grout

Quantity of grout is calculated by the following expression;

(Eq. 5.1)

where    Q;quantity ofgroutm3
V;volumeofgroutingsoilm3
λ;groutingratio0.3→0.4over,Table5.5
J;importance factor0.9→1.2, usual1.0

The values on the table are empirically gotten from the results in past. If necessary, these values should be decided by the injecting field tests, for example, peaty soils etc.

Table 5.5 Standard grouting ratio (λ)　(JGA, 2017)

|  | Sandy soil | Clayey soil |
| --- | --- | --- |
| Double pipe strainer | Over 35% | Over 30% |
| Double pipe with double packers | Over 40% | Over 30% |

Example: For a particular ground improvement site in a sandy ground, ground water controlling was required in a construction. what will be the quantity of grout required for the following conditions of the construction:

The grouted area is 20m*1m and the depth of improved area is 5m

- When using double pipe strainer

- When using double pipe strainer with double packers

Example: For a particular ground improvement site, the grain size distribution curve of the collected soil samples from the site is shown in Fig. ***.

- What type of grout materials will you use for this site

- What type of injection patter will you recommend for this site

(Hint: Use Fig. 5.9)

5.2.5 Applications

Table 5.6 shows the list of various applications of each grouting type with the site conditions.

Table 5.6 List of applications according to types of grout

| Injection Style | Aim of Improvement | Used materials | Improved area |
| --- | --- | --- | --- |
| Single pipe | Rock grouting & filling of existing cavern | Cement suspension & Cement-bentonite suspension | Filling of existing cavern & Filling of hollow parts by pulling out of water-proofing sheet pile |
| Double pipe with strainer | Seepage control of ground water & Strengthening of ground | Solution & suspension (Flash setting & long gel time) | Improvement for bottom ground of shaft, Water cut –off for lack parts of earth retaining wall Protection for ground of shield starting shaft |
| Double pipe with double packer | Seepage control of ground water & Strengthening of ground | Solution & suspension (Long gel time) | Improvement for bottom ground of shaft, Water cut –off for lack parts of earth retaining wall Protection for ground of shield starting shaft (Gravelly ground) |
| Synchronous multi-points | Seepage control of ground water, Strengthening of ground & Anti-liquefaction | Solution (Long gel time) | Underpinning for existing structures, Liquefaction countermeasure, Anti-earthquake reinforcement |

5.3 Jet Grouting

5.3.1 Description

Jet grouting consists of drilling down with a small diameter rod (40.6〜130mm in diameter), and injecting and mixing with a high pressure fluid while rotating and withdrawing the rod. Jet grouting differs from the pre-described permeation grouting. The improvement effect of this method can be expected from the usual injection method, but the construction cost may become more expensive. Especially, this method may be applied when the following conditions are required.

- Ground condition: high N-value, high cohesion, gravelly ground, etc.

- High strength by soil improvement is required (over 3MN/m2)

- Low permeability by soil improvement is required (under 1×10-6～-7cm/sec)

- The area of objective site is narrow and the large construction machine will not be possible to use.

- Soils need to be improved with an existing building in close proximity.

5.3.2 Principle and Mechanism

Basically, three different systems available for performing jet grouting, and sometimes a modified type based on these basic systems are used (Fig. 5.10).

Single pipe system: This is composed of the system to improve the ground by using single tube rod with the monitor which attaches a differential pressure control valve (Fig. 5.11). The objective ground is bored with the single pipe rod to the designated depth, and the grout is jetted out to horizontal direction from a nozzle using the deferential pressure control valve. The rod is rotated and pulled up while the grout is jetted with high-pressure. As the result, soils around the rod are smashed and mixed with the grout, and a solidified mass will be formed with the diameter of about 0.8 m.

Double pipe system: This system is based upon the principle of the single pipe system. If the grout from the nozzle of the monitor is shrouded by the compressed air, the energy of jetting pressure will not be decayed. The achieved diameter of the solidified mass in this case will be more than the single tube system. The working mechanism of double pipe system is illustrated in Fig. 5.12.  Grout with 20 MPa of jetting pressure is jetted out from the inner pipe and 0.7 MPa of compressed air is spouted out from the outer pipe. Based on the data from the past execution work, the diameter of solidified mass obtained from this system found to be varied from 1 m to 2 m.

Triple pipe system: This system differs from the single and the double pipe systems in the sense that the fracturing of the ground is carried out by a high-pressure water jet shrouded with air with an additional low-pressure grout (Fig. 5.13). The high-pressure water of 40 MPa and the air jet of 0.7MPaare jetted to smash soils from an upper nozzle. At the same time, the grout is jetted out to the loosen soil at a pressure of 2 to 5MN/m2 from a lower nozzle. The solidified column diameters achieved with this system are greater than those of the single and double pipe systems, and are usually only up to 1.7m to 2m in diameter.

Table 5.7 shows the characteristics and specifications of each system.

Table 5.7 Characteristics and Specifications of Jet grouting (JAFEC 2014)

| Items | Single pipe system | Double pipe system | Triple pipe system |
| --- | --- | --- | --- |
| Improvable area | Dia. 0.8 m | Dia. 2 m | Dia. 2 m |
| Suitable ground | Sandy ground N<30 Clayey ground c <50 kPa | Sandy ground N≤50 Clayey ground N≤4 (c <50 kPa) | Sandy ground N≤50 Clayey ground N≤7 (c <70 kPa) |
| Obtainable strength | Sandy ground 1.0〜3.0 MPa Clayey ground 0.5〜1.0 MPa | Sandy ground 1.0〜3.0 MPa Clayey ground 1.0 MPa | Sandy ground 1.0〜3.0 MPa Clayey ground 1.0 MPa |
| Constructible depth | 20 m | 25 m | 30 m |
| Specification | Jetting pressure 20MPa Grouting volume 80 l/min Air pressure nil Air volume nil Retrieval speed 2〜6min/m | Jetting pressure 20MPa Grouting volume 60 l/min Air pressure 0.6〜0.7MPa Air volume 1.5〜3.0m3/min Retrieval speed 16〜40min/m | Jetting pressure(water) 40MPa Jetting pressure(grout) 2〜5MPa Water volume 70 l/min Grouting volume 140, 180 l/min Air pressure 0.6〜0.7MPa Air volume 1.5〜3.0m3/min Retrieval speed 16〜25min/m |
| Solidified style | Mixing of soils and grout | Semi-replacement of grout | Semi-replacement of grout |
| Grout materials | Water glass and cement milk | Cement milk & admixtures | Cement milk & admixtures |

Example problem:

The following data was obtained from a geotechnical investigation of a project.

If the depth of improvement is (1) 20m (2) 30m, what kind of system will be preferable?

5.3.3 Procedure

Since the construction procedures of Jet-grouting method are similar, Double pipe system procedure is described as a representative example. Fig. 5.14 show the procedures of double pipe system.

(a) The objective ground is bored with a double pipe rod attached to the drill bit and the monitor at the bottom tip.

(b) The grout and the air pressure are increased and the differential pressure valve is opened. As a result, the air-shrouded grout will be jetted in the horizontal direction.

(c) The double pipe rod is drawn up at designated speed and is rotated at fixed rotation, while the grouting is maintained in the horizontal direction. Since surplus soils and grout liquid will be discharged as the slime during its execution, the treatment of slime should be decided in advance.

In the case of Triple pipe system, the boring is drilled by using casing, because the injection pipe is not attached the drilling bit. After drilling, the casing is withdrawn and the triple pipe is inserted into the drilled hole. The injecting operation is carried out through inserted triple pipe.

5.3.4 Design

The design of Jet grouting is carried out based on the data, which were collected based on the construction record (Table 5.7). If necessary, values for the design are sometimes determined by test works in the site.

As the improved soil strengths by Jet-grouting are standardized according to the soil types and types of Jet grouting (Refer to Table 5.7), the design strength is first determined based on the Jet grouting system adopted and the grouting materials under consideration. Next, the diameter of improved soil mass needs to be determined. The improved diameter, h is expressed as a function of soil strength, jetting pressure, travelling velocity of grout, nozzle diameter and frequency of rotation of the nozzle at a fixed depth as shown in Equation below.

(Eq. 5.2)

The above parameters, except for soil strength, can be determined once the decision of Jet-grouting is made. Therefore, the only variable, which estimates the diameter of improved soil mass, is the soil strength of the objective ground. Equation 5.2, thus, can be represented as follows.

(Eq. 5.3)

When giving the case of Double tube system for example, the relations between the ground strength N value and the improved diameter are shown in Table 5.8 (a) and (b).

Table 5.8 Soil strength and improved diameter of double pipe system (JAFEC, 2014)

- Sandy ground

|  | N≦10 | 10≺N≦20 | 20≺N≦30 | 30≺N≦35 | 35≺N≦40 | 40≺N≦50 |
| --- | --- | --- | --- | --- | --- | --- |
| Dia. of improved area (m) | 2.0 | 1.8 | 1.6 | 1.4 | 1.2 | 1.0 |
| Speed of rod lift (min/m) | 40 | 35 | 30 | 26 | 21 | 17 |
| Volume of grout(m3/min) | 0.06 |  |  |  |  |  |

- Clayey ground

|  | N≺1 | N=1 | N=2 | N=3 | N=4 |
| --- | --- | --- | --- | --- | --- |
| Dia. of improved area (m) | 2.0 | 1.8 | 1.6 | 1.4 | 1.2 |
| Speed of rod lift (min/m) | 30 | 27 | 23 | 20 | 16 |
| Volume of grout(m3/min) | 0.06 |  |  |  |  |

5.3.5 Applications

Fig. 5.15 shows typical applications of Jet grouting. The purposes of these applications are manifold: reduction of settlement, increase of bearing capacity of the ground, increase of stability and liquefaction strength, reduction of active earth pressure, cutting off ground water, and increase of stability in shield tunneling, etc.

5.4 Deep Mixing Method (Mechanical Mixing Method, or Cement Deep Mixing)

5.4.1 Description

Deep Mixing Method (DMM) is an in-situ soil improvement technique with cement or lime as a solidifying material. An auger-style mixing tool with blades attached to the vertical shaft is used and this mixing tool is drilled down into the ground. While rotating and withdrawing of the mixing tool, soils and solidifying materials are mixed in-situ. The treated soil mass will have new engineering properties, such as increased strength, lower permeability, and reduced compressibility than the original soils or fills. Soils which are normally targeted for the improvement by DMM are clayey soils with high moisture contents and saturated fine sand in loose state. On the other hand, the ground which doesn't suit for improvement are consisted of hard ground with very dense materials or stiff materials or the ground with obstructions such as cobbles or boulders. The treatable depth by this method is recorded as 40m. Solidifying materials to be used may be in the form of powder or lump, or in the form of slurry. Various names are used for the group of DMM depending on the type of construction machines and solidifying materials used (e.g.: Mechanical Mixing Method, Cement Deep Mixing, Dry Jet Mixing Method, etc.). All throughout this book, the name DMM will be used.

5.4.2 Principle and Mechanism

Main solidifying materials used in DMM are Portland cement, cementitious solidifying material, lime and lime type solidifying material. The solidified reactions of these solidifying materials are described before (4.2 Surface compaction with cement and lime). That is, it is based on pozzolanic reaction and hydration reaction of those materials. However, this procedure does not involve tamping and compaction steps for the mixed mass after mixing of solidifying material. The deep mixing method is a chemical hardening method, in which a ground improvement agent (cement slurry) is injected into soft ground and mixed with the soil. Hardening results from two types of reactions. First, hydration between the water and cement produces the needle-shaped crystals of ettringite. Next, as hardening proceeds, a pozzolanic reaction occurs between the hydration products and clay minerals forming large numbers of plate-like crystals.

(Eq. 5.4)

Elements affecting the strength of mixed mass after its treatment are summarized in Table 5.9, and, can be conceptually indicated by the following equation (Kitazume and Terashi, 2017).

Table 5.9 Factors that determined the strength of solidified mass (Source: Kitazume and Terashi 2017)

| Items | Descriptions |
| --- | --- |
| Characteristics of solidifying materials Characteristics and condition of soil Mixing condition Curing conditions | Type, quality, mixing water, additives etc. Physical, chemical and mineralogical properties of soil, Organic content, pH of pore water, water content etc. Degree of mixing, timing of mixing/re-mixing, quantity of solidifying material Curing period, humidity, wetting, drying, freezing and thawing, Overburden pressure |

Among these factors, elements, that can be artificially controlled, are matters related to solidifying agents and items related to mixing conditions. Fig. 5.16 shows the relationship between the unconfined compressive strength and the total weight of water summarized by the amount of solidified material mixed and the type of solidifying material (Portland cement, blast furnace cement). This figure shows that the strength of solidified soils decreases with the water content. For soils with water content, wt higher than 200%, increase of cohesion factor does not lead to greater strength. The geo-engineering properties of solidified soil which have been clarified are summarized as follows (Saito, 1991).

Water: The water content of solidified soil is lower than the initial water content of treated soil, and the soil mass is solidified in the state of containing water.

Density: The density of solidified soil is slightly larger than the density of the initial soil state.

Permeability: The coefficient of permeability of solidified soil is smaller than that before its improvement.

Unconfined compressive strength: The unconfined compressive strength and the deformation modulus of solidified soil are increased from the original soil, and its strain at failure is reduced. In other words, ground treated by DMM has higher strength and lower compressibility than untreated ground.

Remarks: The solidified soil has higher strength than the original soil, but has retained large pores at soil structure.

5.4.3 Procedure

Construction principle of this method is to supply solidification material slurry or powder while rotating of the mixing tool with excavating /mixing blades as shown in Fig. 5.17 (Saito, 1991). As a result of these operations, the in-situ soil and solidifying materials are mixed. Fig. 5.18 (Catalogue of JAFEC) shows an example of DMM construction procedures. The soil improvement system is equipped with uniaxial shaft, multi-mixing shafts or chainsaw-like devices (trade name: Trencher).

DMM is basically carried out by the wet mixing procedure which involves injecting solidified materials in slurry form to mix with the soil. Slurry of solidified materials are injected through the hollow stem of the mixing tool. The uniaxial shaft may create a single column of solidified mass, and a multi-mixing shafts may create a set of overlapping columns in a single stroke (penetration and withdrawal). The chainsaw-like device may create continuous panel. The standard mixing tool has two one-meter diameter shafts that produce overlapped soil-cement columns. These solidified masses are applied for large-scale foundation improvement, earth retaining systems, hydraulic barriers, and contaminant/fixation systems.

On the other hand, the dry method employs mechanical mixing which consists of vertical rotary shaft, which consist of vertical rotary shaft(s) with mixing blades at the end of each shaft. In the penetration and/or withdrawal stage, powder-like solidified material is spouted into the ground. The mixing blades rotate in the horizontal plane and mix the soil and solidified materials. In one operation, a column of stabilized soil is constructed in the ground.

5.4.4 Design

The shape of solidified mass by DMM will be generally columnar. Fig. 5.19 (Kitazume & Treashi, 2017) shows the typical installation patterns, which are combined and arranged with columnar solidified mass. The ground improved by DMM is a complicated composite system comprising of stiff stabilized soil columns or elements and untreated soft soil.

As examples, some salient points while designing are described below, using Group column type and Block type cases.

In the case of design for group column type, analysis of slip-failure and the strength of column body should be investigated. When the purpose of the ground improvement is to increase the bearing capacity due to surcharge load, it is necessary to evaluate the bearing capacity using the composite ground theory described in section 4.2 of Chapter 4 (Sand compaction pile method).

In the case of the design for block type, the improved mass can be assumed to be a rigid body. It is necessary to evaluate the sliding and overturning stability for such rigid body, the bearing capacity of supporting stratum under the rigid body and the internal stress in the improved mass.

In general, when the stability of an embankment is the major engineering issue, the block or panel type column installation pattern provides a better performance than the group of individual columns. The stability analysis is much simpler and reliable for the block or wall type of column installation. Contrary to this, the construction of a group of individual columns is far simpler and hence construction time and cost are much favorable for a group of individual columns.

In the wet method for onshore construction, stabilized soil element consisting of two to four round overlapping columns is frequently adopted. The diameter of mixing blade and spacing of mixing shaft are typically 1.0 to 1.3 m and 0.8 to 1.1m respectively, and the cross sectional area of the stabilized soil element is about 1.5 to 5.00 m2. In the wet method for marine constructions, a stabilized soil element consisted of overlapping four or eight round columns has frequently been adopted. The diameter of mixing blade and spacing of mixing shafts are typically 1.0 to 1.6 m and 0.8 to 1.2 m, and the cross sectional area is about 2.2 m2 for four columns arrangement and 4.6 to 5.7 m2 for eight columns arrangement, respectively.

5.4.5 Application

DMM can be used to stabilize ground for many in/or off-shore structures and onshore structures. In addition to its use in improving foundation ground for permanent structures, it also can be used for temporary earth works, such as cut-off walls and shoring walls, as countermeasure for bottom heave, and to ensure ground stability during excavation for construction projects (Fig.5.20). The geotechnical properties of soil-cement varies with soil type and mix design (See: 5.4.2). Therefore, it is desirable to carry out test works at the site before applying DMM. Also, DMM is used to inactivate and fix containments from wastes etc. as a treatment system for chemical reduction and containment.

Applications to clayey and organic soils include increasing bearing capacity, reducing settlement, increasing passive earth pressure, reducing active earth pressure and increasing horizontal resistance of pile and sheet wall. Applications to sandy ground, on the other hand, include bearing capacity improvement, reducing settlement and preventing liquefaction.

Table 5.10 shows typical improvement purposes of DMM for clayey and sandy soils.

Table 5.10 Main applications of DMM

| Types of Site | Target Facilities | Objectives |
| --- | --- | --- |
| Onshore and Offshore On land Sandy ground Waste | Wharf, breakwater, etc. Banking, land development Varieties of facilities Waste disposal | Bearing capacity improvement Bearing capacity improvement, Slope stabilization Liquefaction countermeasure Inactivation and fixation of contaminants |

References

Babasaki, R., Terashi, M., Maekawa, A., Kawamura, M., & Fukazawa, E.,(1996) : Japanese Geotechnical Society Technical Committee Report: Factors influencing the strength of improved soil, Proc. of the 2th International Conference on Ground Improvement Geosystems. Vol. 2. pp.913-918.

CPG Association (2012): CPG Method Brochure, (In Japanese).

Saito, S.,(1991) : Deep Mixing Method, Manual of Ground Improvement Method, pp.367-393, Nikkan Kogyo Sinbunsha.

Kitazume. M., and Terashi. M.: The Deep Mixing Method, 2017, CRC Press

Japan Foundation Engineering and AOI Co. Ltd.: Catalogue

Japan Foundation Engineering Company (2014): Manual of ground improvement with grouting, (In Japanese).

Japan Foundation Engineering Company (JAFEC), (2014): Manual of ground improvement with jet-grouting, (In Japanese).

Japanese Geotechnical Society (JGS) (2009): Theory, Design & Construction of Grouting Method, Maruzen Publishing, Japan (In Japanese).

Japanese Grout Association (JGA) (2017): Design Manual of Grouting Method, (In Japanese).

Japanese Jet Grouting Association (JGA): Technical Materials of Jet Grouting Method (20th Edition), 2012.(In Japanese).

Japan Foundation Engineering Company Brochure, (JFEC, 2017).

Nakanishi, W. & Nakazawa, J. (2006): The Process of Development on Jet Grouting Method and Their Future, Journal of Japanese Geo-technical Association, Vol.54, No.7, pp.10-12, (In Japanese).

Shibazaki, Mituhiro (1984): Essential Knowledge on Grouting (Part 8), Journal of JSIDRE, Aug. 1984, (In Japanese).

Questionnaires – What you have learned.

5.1 In ground improvement, workability (or flow-ability) for wet soil mixing technique is related to mixes limit of liquidity.

5.2. What are the conditions that influence the shape and dimensions of formed jet grouting columns?

Answer: It depends on the type and condition of soils building the subsoil and on technological parameters of columns forming, such as: the injection pressure, the injection rod pulling out and rotation speed, the density of injected cement grout as well as the number and size of injection nozzles.

5.3. What is the problem with jet grouting?

Jet grouting is a widely used technique for soil stabilisation, which provides support to geotechnical structures and buildings. One of the main problems related to this technique is excessive displacement and occasionally high pressures induced on structures in direct contact with the jetted area