Chapter 7 Other Methods of Ground Improvement

Abstract: In this chapter, techniques of Ground Improvement based on special principle are described. In addition, they deal with some methods that have been developed with applications. Especially, Electro-osmosis, Freezing method, Plant-based natural materials on Ground Improvement and Geo-materials utilization with Byproducts/Waste are described.

Keywords: Electro-osmosis, Freezing, Plant-based natural materials, Geo-materials with Byproducts/Waste

7.1 Introduction

This chapter describes Ground improvement techniques based on special principle. In addition, it deals with some methods that have been developed with few applications. Especially, Electro-osmosis, Freezing method, Plant-based natural materials and Geomaterials with Byproducts/Waste on Ground Improvement are described.

Electro-osmosis was developed in the 1940's and was applied to ground improvement work at the same time, but it is economically expensive, so there are few applications. 
However, from the point of research and development, this method is still being researched and developed.

Freezing is Ground improvement technique which solidifies the ground by freezing the pore water of the ground. The artificial frozen ground is superior in waterproof properties and has sufficient mechanical strength on the geotechnical engineering. This method is temporary works of construction and applicable grounds are almost all ground, if it has groundwater.

Plant-based natural materials: Ground improvement techniques which used Plant based natural materials were empirically used from the ancient times, but utilization as Geo-synthetics of them is reevaluated.

Geomaterials with Byproducts/Waste: Use as geomaterials of byproducts/ waste was empirically implemented in the same way. Recently, for the realization of Circulation Society, ground improvement techniques are applied for recycling of byproducts/waste.

.

7.2 Electro osmotic consolidation

7.2.1 Description

Electro osmotic flow is the motion of liquid induced by an applied potential across a porous material, capillary tube, membrane, microchannel, or any other fluid conduit. It is the electro-osmosis method that intends to dewater clay using this principle. Electric osmotic consolidation means to help the consolidation of soft clays by application of electric current. This method was originally developed as a means of dewatering fine grained soils for the consolidation and strengthening of soft saturated clayey soils (Casagrande, 1947).

From Hazarika’s Book

7.2.2 Principle and mechanism

When many clay particles are mixed together in water, particles interact and their unit Micelles overlap each other. There exist several interactive forces (attractive or repulsive) between particles when those particles are brought closer.

*Van der Waal’s Force (Attractive)

*Dipole-Cation-Dipole Attraction

*Cation Linkage (Attractive)

From Wikipedia

*Cation-Cation Repulsive Force

*Anion-Anion Repulsive Force

The resultant force between adjacent particles is the sum of potentially all the preceding attractive and repulsive forces. The magnitude of the force depends on many factors such as the level of surface change, relative spacing, existence and amount of cations and anions, cation valence, etc. Fig.7.1 shows a schematic relationship between interactive forces and relative spacing of two parallel particles. When the space is too close, the resultant is very large repulsive forces due to repelling of both the clay surfaces. The resultant force curve passes through the zero-resultant value. This space is called the equilibrium distance, at which two parallel particles are in balance and establish their stable relative position. The equilibrium distance also depends on many factors, such as electrolyte concentration, ion valence, dielectric constant, temperature, pH of solution, etc., and thus, relative distance of clay particles are influenced by these factors in the environment. The electrostatic relationship occurring at the interface between solid and liquid is called the electrical double layer. Fig.7.2 illustrates the electrical double layer of solid surface. Schematic of double layer in a liquid is at contact with a negatively-charged solid. Depending on the nature of the solids, there may be another double layer (unmarked on the drawing) inside the solid.

A double layer (DL, also called an electrical double layer, EDL) is a structure that appears on the surface of an object when it is exposed to a fluid. The object might be a solid particle, a gas bubble, a liquid droplet, or a porous body. The DL refers to two parallel layers of charge surrounding the object. The first layer, the surface charge (either positive or negative), consists of ions adsorbed onto the object due to chemical interactions. The second layer is composed of ions attracted to the surface charge via the Coulomb force, electrically screening the first layer. This second layer is loosely associated with the object. It is made of free ions that move in the fluid under the influence of electric attraction and thermal motion rather than being firmly anchored. It is thus called the "diffuse layer". Interfacial DLs are most apparent in systems with a large surface area to volume rat, such as a colloid or porous bodies with particles or pores (respectively) on the scale of micrometers to nanometers. However, DLs are important to other phenomena, such as the electrochemical behavior of electrodes.

The DL is closely related to electrokinetic phenomena and electroacoustic phenomena. When electrodes are placed across a saturated clay mass and current is applied, water in the clay pore space is transported towards cathode by electro osmosis. In addition, frictional drag is created by the motion of ions as they move through the clay pores helping to transport additional water. The flow generated by the electric gradient is called electro osmotic flow. It is the process where in positively charged ions move from anode to cathode. ie. Water moves from anode to cathode where it can be collected and pumped out of soil Electro osmotic flow depends on soil nature, water content, pH and on ionic type concentration in the pore water. Due to the applied electric potential the electrolysis of water occurs at the electrodes

2H2O- > O2 (g) + 4H+ +4e- oxidation (anode)

4H2O + 4e--> 2H2 (g) + 4OH- reduction (cathode)

The clay particles have a -ve charge. These -ve charge produce an electro static surface property known as the double layer which creates a net abundance of cations in pore space. Electro osmotic transfer of water through a clay is a result of diffuse double layer cations in the clay pores being attracted to a negatively charged electrode or cathode. The flow generated by the electric gradient is called electro osmotic flow (Fig.7.3). Electric osmosis induces water movement in the fine-grained soil body due to external electric potential gradient (voltage) by establishing a net water flow towards the cathode and creating negative pore water pressure that produces soil consolidation.

Fig.7.4 shows the principle of electro-osmosis. Mobile cations with electrostricted water are attracted to the anode, where water is collected and pumped up for drainage to reduce water content in the field. The anodes consist of iron pipes. The cathodes may merely of iron rods along which the water flows as it escapes to the surface, but should preferably be perforated pipes screened for their full length to permit easier and more rapid escape of the water. Electro osmosis causes consolidation of compressible soils such as clays. The consolidation is accompanied by an increase in strength and generally by a decrease I sensitivity. In addition, the clay becomes fissured. The use of electro-osmosis for altering the properties of clays in this manner has not been as frequent as that for the stabilization of slopes in silty materials.

7.2.3 Designing and Applications

Applicationに汚染土壌の浄化法をいれる

There are few applications in the case of Electro-osmosis method, so designing for them has not been established. Most of the applications to be reported were designed with reference to the results of laboratory test and jobsite trial working. The application has accelerating consolidation for clayey ground and slope stability.

The following application was summarized and cited from the paper of Casagrande et al (1981).

Project name: Second Track Alignment of Canadian Pacific Railways at Clan William, British Colombia.

Object of construction: It was the annex construction of the existing railway, and it was needed the excavating of a 6.7 m depth, the base width of 21 m along two existing railways (Fig.7.5).

Soil condition: Along the depressed section of railway the soil generally consisted of from 5 to 10 feet of soft fibrous peat overlaying 20 to 30 feet of very soft clayey silt, silt and sandy silt, which in turn overlies a stiffer silt or rock.

Stability analysis: A stable excavation would require slopes of 10H : 1V.

The soil should be stabilized sufficiently to permit excavation the area on a 3H : 1V slope.

Selection of method: The electro-osmosis method of stabilization was recommended because it was a proven method that: 1) would stabilize the soil, 2) would provide long term benefits, 3) could be installed with minimal ground support in the swamp, 4) could be adjusted to compensate for changing conditions and 5) would not in any manner deteriorate the environment.

Results of laboratory tests: The soil had an average conductivity of 3×10-4 amps/volt-cm.

The electro-osmosis coefficient of permeability for one dimensional flow was 5×10-5cm/sec per volt/cm, which would permit adequate movement of water through the silt.

It was estimated that a minimum of four months of electro-osmotic treatment would be required to stabilize the excavation at slope of 3H : 1V.

Design: The electro-osmosis design consisted of a row of anodes and row of cathodes installed along each side, at the top of the cut and at the toe of the cut.

The rows of anodes were 10 feet away from the rows of cathodes. Along each row, the anodes and cathode respectively were spaced at 20 feet centers. The anodes and cathodes penetrated to a depth of 50 feet below the ground surface. The anodes consisted of used 34 pound rails. The cathodes of 2” eductor wells with adjacent 1⅟2” steel electrodes encased in 13” diameter selected sand filters. 20 standpipe observation wells were installed. An electrical potential of 150 volts D.C. was applied to the system (op. cit. Fig.7.5).

Results: The improvement in the soil was better than anticipated, consequently the slopes were steepened from 3H : 1V to 2⅟2H : 1V. The excavation and placement of the granular blanket for the 2800 feet section was completed in November 1978.

7.3 Freezing Method (or Artificial Ground Freezing Method)

7.3.1. Description

Freezing method (or Artificial Ground freezing method) aims at solidifying the ground by artificially freezing the pore water of the ground. The frozen ground is impervious to water and has sufficient engineering strength. However, when freezing operation is interrupted, the ground will return to its original state, so this method is limited as a temporary construction method in its application. This method can be applied to most grounds. It is also possible to treat the gravelly aquifer stratum, the soft clay layer and the confined aquifer, which are generally considered difficult to treat. This is a construction technique that is used in the construction of shafts, mines and tunnels to provide temporary earth support and groundwater control when other conventional methods such as dewatering, shoring and grouting or soil mixing do are not feasible. Ground freezing is also used to provide regional groundwater barriers around mining operation for gold and other mineral, oil sand or oil shales. It is often referred to as ground freezing, soil freezing, or freezing wall.

7.3.2. Principle and Mechanism

There are two methods which are applied for Freezing Method (referencing: 7.3.3). In this Section, Brine System in them is described in the example.

The basic principle of freezing process is that installs freeze pipes in the ground and circulates coolant such as calcium chloride brine through freezes pore water in the soil (described later: there is a way of directly injecting of freezing material such as natural liquid gas). When the earth temperature reaches below the freezing point (0℃), pore water in the ground turns to ice. If a row of freezing pipes is placed vertically in the ground and the cooling energy with temperature below the freezing point is supplied into them, frozen soil will be occurred around the pipe, and each frozen soil pillar connects together with time. Frozen soil grows like an annual ring around the freeze pipe. Then frozen pillars become shaped like the frozen wall (Fig.7.6). This frozen wall has geotechnical natures that satisfy some requirements on construction processes. In other words, the frozen wall is formed and reached a thickness sufficient as an impervious and bearing wall.

The geotechnical properties of the freeze ground are described. Fig.7.7 shows relation between unconfined compression strengths of frozen soils and the freezing temperature for them. The lower the freezing temperature becomes, the larger the compression strength of frozen soil becomes. Finally, it is increasing to the strength which is near concrete materials. On the permeability of the frozen ground, if the ground is the situation below the freezing point, its pore water freezes up. Therefore, actually, it of the frozen ground may be evaluated to be impervious.

This method has two weak points that is frost heaving and freezing-thawing settlement. But there is almost no frost heaving and freezing-thawing settlements, especially for the gravel soil. For fine-grained soil such as clay, the frost-heaving and thawing settlements can be predicted by theory so that countermeasures can be adopted to inhibit the frost heaving and decrease the freezing-thawing settlements.

7.3.3 Procedure

Two types of ground freezing methods have been put into practical use, which is the brine system and the liquefied gas system

Brine system

Using refrigeration plant and circulating coolant system. Refrigeration plant cools the brine (calcium chloride solution, specific gravity 1.26 to 1.28) to the temperature of -20℃ to -30℃. The cooled brine is circulated through the freeze pipes where it freezes the ground, then returns to the plant for re-cooling (Fig.7.8).

Liquefied gas system

Coolant, such as Liquefied Nitrogen Gas, is supplied directly through the pipes or to the ground a storage tank and freezes the ground by latent of evaporation (Evaporation temperature -196℃). Where rapid freezing is required, liquid nitrogen is used as the freezing medium, and this can reduce the freezing time to a few days (Fig.7.9).

Comparison of two systems

Liquefied gas system can freeze the ground if ground water flows to high degree, for its faster than brine system. On the other hand it is very expensive with scale and freezing continuing period. Liquefied gas system is suitable for small-scale work of which frozen soil mass is about 150 m3 and freezing continuing is a few days.

7.3.4 Designing

On designing procedures, the brine method where there are many case histories is described.

In case of design of the frozen soil wall which had a purpose of the ground improvement, the purpose of the main construction, location and environmental conditions, the ground condition, the construction period and so on should be reviewed.   The safe and economic plan should be made. Fig.7.10 (Oguro, 2017) shows the flow of the design procedure of them.

7.3.5 Applications

Ground freezing has been used for at least one hundred years (Lightfoot, 1886). The method has been applied to projects such as mines, inclined shafts, tunnels, subways, bridge culverts and building foundations etc.

Especially, the following case histories are listed.

Ground freezing for deep shaft excavation

Ground freezing in the tunneling

Ground freezing to isolate ground water from mining

Ground freezing and tunnel boring machines or shield excavating machines

7.4 Use of Plant-based Natural Materials

7.4.1 Description

This section describes the ground improvement techniques using plants or plant-based natural materials. The procedures of ground improvement using plants have been used empirically from ancient times, but in recent years, it has been re-evaluated from the viewpoint of preventing global warming.

The climate change which is caused by the human activity becomes globally an important environmental problem. Ground improvement methods should be evaluated in the viewpoint of the global warming prevention. In various efforts for them, it is a worldwide trend that low carbon society must be realized. It is to use the plant-based natural materials, in consideration of various measures for the realization of the low carbon society. Trees or woods, which is a typical material of the plant-based natural materials, consist of the organic matter which fixed atmosphere carbon dioxide by the photosynthesis. When these are burned or decayed, these yield carbon dioxide. Since this carbon dioxide was gotten in the growth process, it doesn’t make atmosphere carbon dioxide concentration rise (Fig. 7.11). The plant-based natural materials are evaluated environmentally as the neutral resources of carbon. In such a worldwide technological trends, utilizations of plant-based natural materials for ground improvement are described.

Use of plant-based natural materials for ground improvement is pretty old. Soil reinforcement with river-reeds in the Iranian plateau dates to the fifth millennium B.C. Reed-grids had long been in use for control of coastal and river-bank erosion and can be aptly called precursors to present-day geo-synthetics (T. Sanyal, 2011). The reinforcement earth which used trees, branches, leaves, bamboos and sticks and so on, which are plant-based natural materials, became in the clarifying with the archaeological excavation of the ruins in recent years. In the Great Walls of in China which were constructed in the 2nd century B.C., the reinforced earth structure were made by twigs of the reed and willows shaped like the sticks and were inserted between the regular intervals alternately．When some roads were constructed on the soft ground in ancient Rome, the fascine with reeds was laid on it and pavement stones were placed（http://www.yamazaki.co.jp/）.

In the 7th century at Japan, the dam style bank of Sayama Pond was constructed in using the ancient construction technique of "leaf laying". The leaf laying method is a sort of ground improvement for stably holding the embankment body when embankment is performed, and is based on the same principle as the soil reinforcement of modern geosynthetic. When construction of earthen structures such as embankments, the thin layer compaction method was empirically carried out by spreading soil materials to a thickness of about 10～15 cm and compacting them. The leaf-laying method is a procedure of laying plant-based branches and leaves between thin soil layers of each step. It is considered that these laying leaves promote drainage between the embankments and serve as a scaffold for workers. After the embankment is constructed, leaves materials will act as the shear resistance to slip failure of it. The technical lineage of the embankment construction of Sayama Pond is thought to lead from Anfeng Pond in China (B.C. 598-591) to Byeokgoljae in South Korea (4th century). Fig.7.12 are examples of the leaf-laying method discovered by the archaeological research (Oosaka-sayama Board, 2014).

年号記入

The earthen walls of traditional Japanese houses use mixtures of earth and cutting rice straws, but this cutting rice straws was designed to increase the strength of earthen walls. Applications of cutting rice straws were to reinforce walls, prevent cracks, improve bending strength, and also improve workability.

Different methods of soil stabilization with plant-based materials were followed in India from the pre-historic and Vedic period (up to 600 B.C) to the period of Shilpa Shastra (1500 A.D.). Hazarika (      ) summarizes and examines some of the ground treatment methods developed in ancient India and their relevance and significance to the modern ground improvement.

これ以降1頁分先生のレジュメを丸写ししています。適当に変更してください。

Making of wall plaster

The process involves the following five steps:

- Fine sand is washed thoroughly first to remove any dust in it.

- Hydraulic lime prepared by burning shells, conches etc., is then mixed with the sand in equal proportion.

- A mixture resinous exudation of fig trees, triphala, seeds of masa and pre-boiled flour of gram or maize are taken in equal proportion in which water is added in proportion of 16:1. The mixture is then boiled so that water remains in 1:1 proportion.

- This mixture is then mixed with the lime and sand mixture obtained in (2) and beaten thoroughly.

- The whole mixture is rested for a period of three months, and afterward again so as to make it as smooth as butter and form the plaster. Such plaster was applied to walls, which are believed to have high resistance to the atmospheric weathering.

Stabilization of soils for preparing Idols

Idols of gods and goddesses of Hindu religion were prepared from stabilized soils. The main purpose of such stabilization was to make the idols waterproof so that the water used for washing the idols do not affect their longevity. This kind of stabilization technique involves the following five steps.

- Right type of soil was first selected, and then mixed cow’s milk, yoghurt, butter and linseed oil. While cow’s milk (sacred in Hindu tradition), yoghurt, butter were supposed to be added as flocculating agents, linseed oil was used as waterproofing agent.

- Lime, gravel, rock and iron fillings were then added in equal proportion to the mixture prepared (1). These agents were added to increase the compressive strength of the mixture.

- In the mixture obtained in (2), a mixture of turpentine, resinous exudation of Sala tree, saffron paint, kusta (a sort of poison), and a kind of grass called Kunduru was added. These substances react with soil chemically and make it waterproof. The whole mixture was then beaten smooth.

- Then soils collected from the confluence of two rivers were added to the above mixture obtained in (3).

- Finally, the whole mixture was beaten smooth for a period of one month, which produces a stabilized soil. It is started that such a soil becomes as hard as a stone or iron.

Capsule for melting metals

The annular capsule made of two layers: inner layer and outer layer. The outer layer was made of stabilized soil. The stabilized soil was prepared by mixing the soil with rice husk, cotton and salt and then thorough grounding of the mixture.

7.4.2 Basic Concept for Plant-based Natural Materials and Ground Improvement

Because plant-based natural materials are evaluative with carbon neutral materials as above-mentioned (Fig. 7.11), the usages of them for the ground improvements are desirable from the viewpoint of the low-carbon society.  At this stage, the following three items are thought as usages of plant-based natural materials for the ground improvement.

Utilization as it maintained the form of plant-based natural materials

Utilization of processed goods from plant-based natural materials

Utilization of microbial functions

The present state of each utilization is described below in the summary.

7.4.3 Utilization by original form of plant-based natural materials

Table 7.1 shows examples of using plant-based materials for ground improvement while maintaining the shape of plants growing in the natural state. Currently, there are two styles of their applications. One is to cut the felled state to a predetermined length according to the purpose of use, and the other is to mix the shredded chips into soil.

When plant-based materials are applied as materials for ground improvement, there is a concern that the plant will decay. The conditions for wood decay are temperature, moisture, oxygen, and nutrients, but when the depth is deeper than the groundwater level, the wood becomes nearly saturated and the oxygen required for the growth of decay fungi is insufficient. For these reasons, the decay of plant-based materials hardly progresses below the groundwater level.

Table 7.1 Applications (1) of Plant-based Natural Materials

| Main category | Name | Description |
| --- | --- | --- |
| Stem and Twig | Stick/twig/bush-wood Log-pile Bamboo | Geosynthetics (fascine or fagot) Floating foundation or piling Floating foundation |
| Chipping fragments of plants | Rice straw Barley/Wheat straw | Chipping plant-material fragments for mixing with soils |

7.4.4 Utilization of processed goods from plant-based natural materials

On this item, Sanyal (2011) reported the applications for the geosynthetic functions on leaves from Indian plants. Table 7.2 shows the available fibers of plant-based materials as the reinforcement function by consulting this report. Basically, these ways are using the clothes as the ground reinforcement material, which were made from vegetable fibers

Fruit Fibers extracted from the fruits, are light and hairy.

Bast Fibers are found in the stem of the plant its strength. Usually they run across the entire length of the stem and are therefore quite long.

Leaf Fibers extracted from the leaves are generally rather rough and sturdy.

Stem Fibers (Bamboo fibers) are separated when bamboo pieces cut into chips are boiled in the dilute solution of sodium hydroxide (Ikeda, 2009).

Table. 7. 2 Applications (2) of Plant-based Natural Materials (Original: Sanyal, 2011)

| Main category | Name | Description |
| --- | --- | --- |
| Fruit Fiber | Cotton Coir | Cotton is unsuitable for geosynthetics by low tensile strength. Coir is being extensively used as geosynthetics. |
| Bast Fiber | Jute Flax Ramie Hemp | Jute fibers are suitable for geosynthetic construction. Flax is good heat conducting properties. Ramie is a durable fiber. Hemp fibers are strong and have high resistance against water. |
| Leaf Fiber | Sisal | Sisal sturdy and strong fivers against moisture and heat. |
| Stem Fiber* | Bamboo | Bamboo fibers exhibit high water absorption and dry quickly. |

*mark: Added by authors

The table lists mainly Indian plants, but there may be other types of foliage available in some regions. Most of them in the table are processed into cloth and used as reinforcing materials for reinforced soil, but jute ropes of long fibers are bundled and used as drain materials for Vertical Drain Method (See Section 3.4). Regarding the application of bamboo fibers, it has been reported that the engineering properties (compressive strength, bending strength, tensile strength, tensile toughness, etc.) of the solidified soil cement are increased when bamboo chips are mixed with the cement soil (Huang, et al 2011).

7.4.5 Utilization of microbial functions

Although it is not directly using plant-based natural materials, ground improvement is being attempted using microorganisms of biological origin, so the summary is quoted below (Kawasaki, 2015).

The following four items are listed for the possibility of ground improvement applying microorganisms.

Bioremediation: To repair the contaminated ground with toxic substances.

Bio cementation: To increase the ground strength.

Bio clogging: To reduces the permeability of the ground

Bio desaturation: To reduce the saturation of the ground as a measure against liquefaction.

In nature, minerals such as calcium carbonate, silica, and calcium phosphate are produced by living organisms. These biominerals can be applied as solidified materials for ground improvement. As an example, the cementation technique applying calcium carbonate is quoted below (Kawasaki, 2015): Currently, it is at the laboratory level, but the principle of this method is described below.

Calcium carbonate, which was separated by urea-splitting bacteria, solidifies the ground. Firstly, the culture solution of urea-splitting bacteria is injected into the ground. And then, nutrient salt, which contains calcium chloride and urea etc., is regularly grouted into the ground which contains culture solution. As a result, calcium carbonate is precipitated in the ground and expresses the solidification effect. This method is called Microbially-induced carbonate precipitation and the using bacteria is Sporosarcina pasteurii (Bacillus pasteurii).

Now, these studies were conducted mainly in the laboratory and may lead to unprecedented new understanding, discoveries, and development through cooperation between microbiology and geotechnical engineering field in the future.

7.4.6 Applications

Applicationに以下の2例を引用しました。これで良いかご検討ください。

In this section, the ground improvement which used Plant-based natural materials is described. Refer to above-mentioned related chapter about these design and these construction procedures, because the conventional inorganic materials in ground improvement were changed into the plant-based natural materials. For reference, some case histories of ground improvement by plant-based natural materials are described below:

T. Sanyal & N. KR. Mukherjee (2011)

“Jute geotextile in rural roads – Case Study”

The main objective of R&D project was to evaluate the technical advantages of Jute Geotextile in rural roads. The advantages are supposed to be evaluated for individual functions of JGT as components of road structure as outlined below.

Advantage as a separation layer

Advantage as a drainage layer

Advantage as supporting system for construction of embankments on soft ground

Advantage as improvement in CBR of sub-grade

Advantage as facilitator of growth of vegetation on slope

Advantage as capillary cut-off

Installation method of JGT

The approved JGT was laid on a 50mm sand cushion overlain by a sand-cover of the same thickness. The sand-layer was placed over the prepared sub-grade. JGT was stapled at interval of 750mm with overlaps of 150mm crosswise and 300mm longitudinally. Staples used were of U-shaped nails (11 gauge) or broad-headed country nail of 150mm length as available. The purpose of the sand-cushion was to prevent probable puncture/damage to the fabric during rolling of the overlaying granular sub-base and to act as a supplementary drainage layer.

Benkelman Beam tests indicate satisfactory overall performance of the pavement indicating effectiveness of JGT as soil-improving natural technical textiles.

G. Basu, A. N. Roy, L. Mishra, R. Chakraborty and S. K. J. Abbas (2011)

Novel Natural Fiber-based Composite-structure Geotextiles for Protection of River Bank - A Case Study –

Bank erosion causes inconceivable damage to human habitation and property every year. Looking into the perennial problem and non-availability of indigenously produced geotextiles for specific use, a set of novel geotextile fabrics using jute and jute-coconut fiber blended yarn separately and polyolefin tape yarn has been developed. Some composite structured/layered-structured geotextiles have been developed. The fabric samples contain more than 70% (wt/wt) natural fiber.

A successful field trial was conducted for protection of a part of the bank of Mayurakshi River (rain-fed river) at West Bengal using the developed geotextiles based on the principle of using geotextiles as reinforcing materials for stable grass-turfing. The vertical height and angle of gradient of the bank were approximately 9.0m and 60deg. respectively. All the materials used for execution of laying-work of geotextiles were procured from adjacent locality. The work-force was also appointed from the nearby villages. A total shower (till laying of geotextiles) during monsoon was recorded as nearly 140cm and then at the end of full monsoon period, even after release of stored water from Massanjore dam through Telpara barrage @125,000 cusec (plus additional 35,000 cusec from local catchments due to a spell of spear-headed shower for continuously three days during the same period), and zero erosion of the part of the river-bank under trial was observed. Vegetation had been established. While, on the rest of the part (where geotextile was not been used), signs of major soil erosion including rain-cuts (Number of rain-cut – 64/100m length of river-bank) were clearly visible. In case of all-PP geotextiles, patchy grass vegetation, slipped/washed-out soil cover and torn-off places due to cow hooves were observed.

7.5 Geo-materials Utilization with Byproducts and Waste

7.5.1 Description

In 2015, UNDP (United Nations Development Programme) adopted SDGs17, which had the purpose to promote poor extermination, unequal correction, sustainable development and so on. SDGs are a major theme of what we should do to develop the economy while protecting the global environment. Among the goals of SDGs17, Goals 12 and 14 are considered to be the goals that the ground improvement technical field can directly contribute to (e.g., Wikipedia 2021);

Goals12 “Responsible Production and Consumption.”

“Ensure sustainable consumption and production patterns”

Goals14 “Life below Water.”

“Careful management of this essential global resource is a key feature of a

sustainable future.

In our actions on achieving two goals, we consider matters related to waste disposals and treatments. Currently, human beings generate a large amount of waste by their lives, but they face the problem of polluting the environment if it is not properly treated. 3R Actions, which are activities to reuse waste as a resource, to reduce the waste itself and to recycle waste as materials, are one of the behavioral forms of the SDGs. Furthermore, these actions can be said to be an effort to solve problems such as depletion of global resources, global warming, and marine pollution.

3R Actions, that form the basis of the waste problem, are as follows:

Reduce: Reducing the generation of waste,
Reuse: Repeating use of materials,

Recycle: Reusing waste as a resource

Considering the ground improvement techniques that can directly contribute to the SDGs, it is the contribution of the SDGs to Goals12, and as a result, the contribution of Goal14. In concrete terms, it is meant to utilize the ground improvement techniques for the reuse and the recycling of an industrial by-product and a waste. That is to say, ground improvement techniques can make by-products and wastes to geo-materials. Because geo-engineering properties of some industrial by-products are higher than the earthen materials and some of them have self-hardening properties, some of them can be reused as geo-materials directly.

On the other hand, wastes which are produced by the human life exist in a wide range of their compositions and their forms. If applying the principle of the ground improvement for the processing and the disposal of these wastes, these, too, can be used as geo-materials.

Recently, large scale natural disasters are occurring by the global climate change. As for the example of the large scale natural disaster, earthquakes, tsunami (seismic sea wave) which are accompanied by earthquakes, the typhoon, the flood, the tornado, the volcano eruption and so on can be listed up.　After the large natural disasters, the large quantity of miscellaneous debris remains in the damaged area. These are divided in the name with the disaster waste, which a large amount of waste such as concrete debris, wood chips, and waste of many home facilities are generated by natural disasters. In particular, among various natural disasters, disaster waste which deposited after an earthquake, flood, or tsunami is composed of a collection of miscellaneous substances mainly composed of soil. If ground improvement techniques are used for the means for disposals and treatments of these, these will become able to be diverted into geo-materials, too. Ground improvement techniques can be called the technology which is useful to make the circulation materials from various waste

7.5.2 Practical Use of Byproducts/Waste

The technical term "artificial geo-material" is listed in the systematic name by the Method of Classification of Geo-materials for Engineering Purposes (JGS 005-2000) of the Japanese Geotechnical Society. The artificial geo-material is defined as artificially processed or produced, and subdivided into improved soil and waste. Table 7.3 shows concrete examples that are considered as artificial geo-materials (Omine, 2017).　Table 7.4 (Omine, 2017) shows the raw materials of those exemplified in Table 7.3. From these tables, it is clear that ground improvement techniques plays a major role in the materialization of artificial geo-materials.

Table7.3 Examples of Artificial Geo-materials (Omine, 2017)

| Classification Concept | Example |
| --- | --- |
| Classification by Original Material | - Solidified soil with Chemicals - Available Waste - Recycled Waste - Industrial Goods - Combined Soils with Other Materials |
| Classification by Function | - High Strength - Light-weight - Fluidity - Toughness - Elution Inhibitor for Harmful Substance - Permeability or Water Holding |
| Classification by Preparation | - Stabilization by Chemicals - Dehydration and Drying - Particle Size Control and Mixing - Burning - Melting - Foaming |
| Classification by Use | - Banking - Backfilling - Refilling - Reclamation - Sand Substitute - Water Stop Materials |

Table7.4 Artificial Geo-materials based on row materials (Omine, 2017)

| Category Name | Example |
| --- | --- |
| Stabilized Soil | Cement stabilized soil Bubble-mixed lightweight soil Foam beads mixed soil Fluidization-treated soil, etc. |
| Waste | Incineration ash Steel slag Coal ash Waste wood Waste glass Waste tire Waste plastics, etc. |
| Recycled material | General waste molten slag Waste glass Granular solid material Carbonized materials, etc. |
| Industrial product material | Polymer materials Expanded Polystyrene Urethane foam etc. |
| Mixed soil with different materials | Mixed soil with tire chips Fiber mixed soil Bentonite mixed soil, etc. |

7.5.3 Disaster Waste

General artificial geo-materials are discussed in 7.5.2, but the geo-materialization of disaster waste has different properties from general artificial geo-materials and will be discussed separately in this section.

As the typical example of the large-scale natural disaster, there are below:

the flood, the landslide and the tornado which are caused by the meteorological phenomenon,

the ground liquefaction, the detritus avalanche, the landslide and the

tsunami which are caused by the earthquake,

the lava flow and the pyroclastic flow which are caused by the volcanic

explosion.

When the energy of the mighty nature such as the earthquake and the flood attacks directly a city and so on, many structures and many buildings are fallen down by the impacting power with the natural energy. Many constructional members of the structure are fractured, and furniture and consumer electronics do not work. As a result, these are accumulated in the designated area as the abandonment unnecessary materials. This accumulation is called a disaster waste.

Typical examples of the disaster waste are shown as follows.

Mixtures with concrete waste:

These are the concrete fragments and concrete lump by dismantlement or

Removal of concrete structure and so on, sometimes reinforcing iron bars

mix with them.

Mixtures with asphalt waste:

These are mainly composed of the asphalt lump which occurred in removal of damaged asphalt pavement roads.

Mixtures with metallic scraps

These are fragments and scraps from steel frames, iron bars, metallic sashes and steel shutters accompanied by dismantle of damaged buildings or structures, sometimes including damaged machineries or damaged household electric appliances.

Mixtures with wooden scraps

These are scrap woods such as the waste wood (the pillar and beam material and so on), the interior fabric, and unnecessary wooden furniture in case of dismantlement of damaged wooden buildings by disasters, and was washed away by the flood and the tsunami.

Mixtures with combustible waste

These mean the mixture which contains combustibles (scrap woods, the disposed plastic goods, waste papers, waste fibers and so on).

Mixtures with non-combustible waste

These mean the mixture which contains non-combustibles (rubbles, waste glass, waste china wares, bricks, waste tile and so on).

Mixtures with waste soil

These are sediments of the landslide, and sediments by Tunami or floods. Depending on the characteristics of the disaster area, furniture, housewares, inappropriate waste for combustion, chemical substances, harmful substances, etc. are mixed in them.

7.5.4 Circulation Materials

Materials to judge availability in the waste are defined as being "circulation resources or circulation materials" and following materials are shown: (e.g., Basic Low for Establishing a Recycling-based Society, Government, 2000).

Construction by-products: construction surplus soil, waste concrete lump, waste asphalt-concrete lump

Industrial by-products: slags, waste glass, waste tires, waste plastic

Table 7.5 shows examples of circulation materials (Omine, 2 017）.

Table 7.5 Circulation materials and those Utilizations (Oomine, 2017)

| Main types | Detail items | Utilization |
| --- | --- | --- |
| Construction by-products | Soil generated by construction Dredged soil Asphalt-concrete block Concrete block Wood chip generated by construction Construction sludge | Banking & Backing materials Banking materials by solidifying Aggregate for asphalt mixtures Recycled stone and sand Fuel, compost & paper pulp etc. Banking by solidifying, aggregate |
| Industrial by-products | Steel slag Coal ash Paper sludge incineration ash Waste gypsum board Waste glass Waste tires Waste plastic Oyster shell etc. General waste molten solidified Sewage sludge melt solidification | Banking & pavement materials Fly-ash, clinker-ash & geo-material Ground improvement materials Ground improvement materials Materials for Formed waste glass Mixed soils with waste tire chips Light-weight soils Ground improvement materials Materials for reclaimed ground Aggregate for concrete |
| Revival materials from disaster waste | Recycled concrete crushed stone Sorting soils Sorting soils from disaster waste Sorting soils from Tunami deposits | Recycled aggregate for concrete Banking materials or backfilling-materials |

Tire-wasteの項はbook Bのハザリカ論文イントロを引用,適宜削除、

7.5.5 Applications

Various methods have been proposed and tried for the reuse of industrial by-products and wastes as ground materials. Tire waste and disaster waste are taken up as typical application examples and described below.

- Tire-waste materials (Hazarika et al., 2022)

Scrapped tire, which are derived materials such as tire chips and tire shreds, can be categorized as three dimensional geosynthetics. Three geotechnical applications of tire chips and tire shreds are considered now as follows:

(1) tire shreds to improve drainage of ground,

(2) sand mixed tire chips cushion to mitigate earthquake damage,

(3) tire chips mixed cement treated clay to improve toughness and ductility.

It was observed that tire shreds can maintain high permeability of ground, even under high compressive load. When tire chips and/or sand mixed tire chips are used as compressible cushion, not only the dynamic load against a structure but the dynamically induced permanent displacement of structure could also be significantly reduced.  On the other hand, mixing tire chips with cement treated clay yields toughness to the geo-material, and, thus provides resistance against development of cracks during deformation.

An estimated 104 million of scrap tires are generated annually in Japan, out of which 90% are recycled for thermal, material and retreading purposes. A major share of scrap tire recycling, however, goes to thermal recycling, a process that generates carbon dioxide (CO2). The amount of CO2 emission by material recycling of scrap tires, on the other hand is only 1/4 that of thermal recycling. Engineers and researchers, therefore, have been undertaking efforts to utilize the scrap tire derived materials as geo-materials. To date, sustained efforts by researchers around the globe have led to many innovative recycling techniques of scrap tires in engineering applications. Research on scrap tire derived products (such as tire chips and tire shreds) as geo-materials has been conducted since the early 1990s, mainly in the United States and Canada. Pioneering research initiated by Humphrey (1998) has resulted in the expansion of scrap tire related research worldwide, especially to the Asia pacific region and Europe. In Japan, research on such geo-materials started around 2000 (Karmokar et al. 2002). Since then, Japan has seen a tremendous progress of the research on material recycling of tire derived materials　with many innovative applications such as cushioning technique (Hazarika 2007, Hazarika et al. 2008). A moral boost to the research and applications on tire derived geomaterials came from the research by Prof. Edil of the United States (Edil 2007), which effectively silenced the critiques that often raised the negative environmental effect of using such materials in geo environment..

Advantages of using scrap tires in civil and geotechnical engineering practices are manifold. They are lightweight, have high vibration absorbing capacity, high elastic compressibility and high hydraulic conductivity, and also they possess a very good thermal isolation potential. In addition, they perform in three dimensions when used as geo-synthetics. Due to myriads of such potentials that these three dimensional geo-synthetics posses, in many applications they are becoming preferred materials as compared to other marketed geo-synthetics products. New techniques have continued to emerge towards utilizing these advantageous characteristics for practical purposes (Yasuhara et al., 2006). Applications for utilizing the tire-derived geo-materials can be broadly classified into two categories:

- Stand alone application (use of tires and tire shreds/tire chips as it is),

- Composite application (tire chips mixed with soils and/or other materials).

Both applications have many potential benefits. The Japanese experiences in both the category are described in Yasuhara et al. (2007). One of the later category applications is to mix tire chips with soils, and use them for backfilling purposes (Hazarika et al., 2007). Triaxial test results of Hyodo et al. (2007) have shown that tire chips mixed sand can prevent the liquefaction of loose sandy backfill due to their three dimensional reinforcing effect, if proper mixing percentage is selected. This has also been proven through model shaking table test by Hazarika and Yasuhara (2008). These element and model testing have indicated that by mixing 50% (in volume) of tire chips with sand, liquefaction could be prevented even for a backfill with relative density as low as 50%. Various mechanical properties of sand tire chips mix have been reported in Edil & Bosscher (1994), Ghazavi (2004) and Youwai & Bergado (2003). Yasuhara et al. (2004) adopted a different approach of utilizing tire chips, in which tire chips are added to cement stabilized soils. Their research has demonstrated that the toughness of cement treated clay can be improved by adding shredded tire chips, and thus can be utilized effectively in soil structures where deformations are anticipated. Varieties of other geotechnical engineering applications of tire chips and tire shreds have been reported elsewhere (Bosscher et al, 1997; Tweedie et al, 1998, Humphrey and Tweedie, 2002).  Whatsoever, the applications may be, the internal structure of the deformation mechanism needs to be identified properly using non-destructive technique such as X-ray CT scanning (Otani et al., 2002). Such approaches have been described in Kikuchi et al (2006) and Mitarai et al (2007).

Amongst those possible techniques of utilizing the scrap tires, this paper introduces three potentials of tire derived products for geotechnical applications. Three specific applications of tire derived materials such as tire chips and tire shreds are described: (1) tire shreds to improve the drainage (stand alone application), (2) sand mixed tire chips cushion to mitigate the earthquake related damage (composite application) and (3) Tire chips mixed cement treated clay to improve toughness and ductility (composite application). The techniques, their verification through model testing and element testing as well as case study applications of some of these techniques from the Japanese experiences have been described in the following.

Tire Shreds as Drainage layer under High embankment

This research was framed to explore the drainage/filtration applications of shredded scrap tire materials (tire shreds). A full-scale field trial on the use of scrap tire shreds under high embankment was undertaken in Hokkaido, Japan (a site of East Nippon Expressway Co. Ltd. near Houbetsu east tunnel). However, extensive permeability tests on tire shreds under simulated field conditions were required before hand. Therefore, permeability tests were carried out using a prototype apparatus designed specifically for evaluating drainage/filtration potentiality by considering the compression characteristics of the tire shred mass. It may be argued that tire shreds are compressive in nature, and hence under vertical load the drainage potentiality would alter according to the levels of compression. Thus, evaluating the drainage behavior of tire shreds essentially needs the compression phenomenon of the tire shreds to be taken into the account. Compression tests and permeability tests were, therefore, at first conducted at a laboratory scale, which are described in the following

2) Disaster Waste Materials (Sakakura, 2017)

As mentioned above, disaster waste is a mixture of various substances. The first treatment stage of disaster waste is the accumulating and the sorting work for them, but working flow of the disposal of the tsunami deposits, which much soil disposal may be needed in the various disaster waste, is considered below as the application example.

Figure 7.13 shows an example of the disaster waste treatment flow, including tsunami deposit, After the disaster, the first step of working is the accumulation of disaster-wastes which are deposited and scattered around damaged areas. Construction machineries will basically be used for the accumulating works of disaster waste. The accumulated mixture is carried at the primary temporary storage site and roughly sorted by appearance, but the sorting work is carried out by heavy construction machineries. The rough-sorted mixtures are transported to the secondary temporary storage sites, and then re-sorting works are carried out by methods such as crushing, sieving, and gravity concentration, etc. For example, they can be roughly divided into concrete scraps, metal scraps, and wood scraps, etc. At this stage, they are sorted into a non-combustible mixture or a combustible mixture. The most of combustible mixtures are incinerated. Soils obtained by sorting, tsunami deposits that have been sorted and ash after incineration are used as geo-materials. Ground improvement techniques are applied in this process if necessary. Ground improvement techniques are applied to the work of the underlined Gothic font in Fig.7.13.

References

Amgasaki City (2007): Diagram of History of Amagasaki City

Basu, G., Roy, A. N., Mishra, L., Chakraborty R. and S. K. J. Abbas, S. K. J. (2011): Novel Natural Fiber-based Composite-structure Geotextiles for Protection of River Bank - A Case Study, Geosynthetics India ’11, 23-24, September, IIT Madras, Chenmai, pp.48 - 59

Casadrande, L., (1947): The application of electro-osmosis to practical problems in foundations and earth works, Build. Res. Tech. Paper No.30, London, 16pp.

Casadlande. L., Wade, N., Wakely, M. and loughney, R., (1981): Electro- Osmosis Projects, British Colombia Canada, Proc. 10th ICSMFE, pp607-610.

出版物、年号、ページを記入してください

Environment Government of Japan (2000): The Basic Law for Establishing the Recycling-based Society

Hazarika, H. (    ): Ancient Practice of Soil Treatment in India ************

Hazarika, H., Kuribayashi, K., Kuroda, S., Yasuhara, K. and Kamokar,K.,(2022): Chapter 10 Applications of Waste Tires for Protection of Embankments in Northern and Northeastern Japan

http://www.yamazaki.co.jp/data/school/pdf/kd211.pdf

Huang, H., Jin, S. and Yamamoto, H. (2011): Study on Strength Characteristics of Reinforced Soil by Cement and Bamboo Chips, Applied Mechanics and Materials, Vol.71-78, pp.1250-1254.

Humphrey (1998)

Ikeda, Y. (2009): Characteristics of Bamboo Fiber and Development of its Uses, Sen’i Gakkaishi (Bulletin of the Society of Fiber Science and Technology, Japan), Vol.65, No.1., pp.45-48.

Ishibashi, I., and Hazarika, H., (2010): Soil mechanics fundamentals, CRC Press, New York.

Ito, Y., and Yoshida, S., (2016): Artificial ground freezing method and its application, Transition of ground improvement technologies in Japan, Journal of the Society of Material Science, Japan, Vol.65, No.12, pp.883-889.

JGS (2013): Survey, Design and Construction in Ground Improvement, (Geotechnical Engineering Practice Series 31), pp.160-161. (In Japanese).

Japanese Geotechnical Society (2009): Standards of Japanese Geotechnical Society, ISBN 978-4-88644-083-9, (In Japanese).

Kawasaki, S. (2015): Present Status of Ground Improvement Technologies Using Microbial Functions, Journal of MMIJ. Vol.131, pp.155-163.

Karmokar et al. (2002):

Lightfoot, T. B. (1886): On refrigerating and ice-making machinery and applications, Proceeding of the Institution of Mechanical Engineers, pp.201-261.

Nara National Research Institute for Cultural Properties (2016.6.16): Nabunken Blog.

Oguro, H., (2017): Outline and case histories on ground freezing method, Monthly Magazine Suisin Gijutu (Monthly Pipe jacking method), Vol.31, No.10, pp.36-37. (In Japanese).

Oomine, K., (2017): Trend in Development of Artificial Geomaterials and Future Prospect, Geotechnical Engineering Magazine (JGS), Vol.65, No.9, pp.1-3 (In Japanese).

Oosaka-sayama Board of Education (2014): Report of Sayamaike Scientific Research Project.

Sakakura, H., (2017): Geotechnical applications of Industrial by-products and Disaster Waste Materials, 7. Disaster Waste Materials, Geotechnical Engineering Magazine (JGS), Vol.65, No.9, pp.32-39. (In Japanese).

Sanyal, T. (2011): Natural Fibers as Geosynthetics, Geosynthetics India ’11, 23-24, September, IIT Madras, Chenmai, pp.KN44-KN56.

Sanyal, T. and Mukherjee, N. KM. (2011): Jute Geotextiles (JGT) in Rural Roads – Case Study, Geosynthetics India ’11, 23-24, September, IIT Madras, Chenmai, pp.27 - 32

Wikipedia (2021):http://www.un.org/sustainabledevelopment/news/communications-material/

Questionnaires – Practicing what you have learned.

7.1 Why are the clay surfaces charged negatively? What is the importance of the absorbed water layer around clay surface?

# 7.2 Is there any industrial waste material that can improve engineering properties and reduce swell-shrink behaviour of expansive soil by stabilization?

# 7.3 What are uses of waste in geotechnical engineering?